Simplex Constraints, Spatial Generalization, and the Regressor–Detector Gap in Machine-Learning Surrogates for CALPHAD Phase-Fraction Prediction

Sina Mousavia, Hesamedin Ayatib*, Erfan Pirhadi Nouric

a Department of Computer Science Faculty of Statistics, Mathematics and Computer Science Allameh Tabataba'i University Tehran, Iran

b Department of Materials Engineering, Tarbiat Modares University (TMU), Tehran, P.O. Box 14115-143, Iran

c School of Metallurgy and Materials Engineering, College of Engineering, University of Tehran, Tehran, Iran

Abstract:

Machine-learning surrogates can accelerate CALPHAD equilibrium calculations by several orders of magnitude, yet predicting multi-phase fractions introduces a strict physical requirement: outputs must reside on the probability simplex to conserve mass. Despite its necessity, a consensus on enforcing this constraint remains absent. To address this, we systematically benchmark six neural network output architectures against four classical baselines across 44,397 mass-balance-validated equilibria from five Fe-based ternary systems (Fe–Cr–Ni, Fe–Cr–Mn, Fe–Cr–Mo, Fe–Cr–V, Fe–Mn–Ni). We demonstrate that structurally constrained heads natively enforce mass balance to float32 precision without compromising continuous regression accuracy. Furthermore, predictive performance is topologically dependent: constrained Multilayer Perceptrons (MLPs) perform best in systems with smooth phase coexistence and Random Forests perform best in systems with sharp, binary boundaries, with statistical ties in the remaining systems. By utilizing size-matched random controls and a region-matched reanalysis, we separate data-volume penalties from spatial domain shifts across contiguous interior holdouts and strict one-sided extrapolation tasks. While MLPs degrade more gracefully during in-hull shifts, strict out-of-range extrapolation degrades error by roughly an order of magnitude across all evaluated model families; the temperature protocol is additionally limited by the closed phase basis, as the liquid phase is absent from the near-side training data in four of the five systems. Additionally, we characterize a critical "regressor-detector gap," revealing that models minimizing aggregate regression error fail to detect rare trace phases and degrade further under distribution shifts. Finally, detailed reporting of failed constraint mechanisms—including sparsemax, soft loss penalties, and residue closure—yields concrete design guidance for future materials informatics.

Keywords: CALPHAD; Machine learning surrogate; Simplex constraint; Spatial generalization; Phase fraction prediction; Iron alloys.

# Introduction

The paradigm of Integrated Computational Materials Engineering (ICME) has fundamentally transformed modern alloy design by treating materials development as a concurrent, requirements-driven engineering process[1, 2]. At its core, ICME establishes tight, multiscale mathematical linkages across the processing–microstructure–property–performance chain, effectively replacing empirical trial-and-error with top-down computational design [2]. Within this framework, computational thermodynamics serves as the foundational connective tissue . The CALPHAD (CALculation of PHAse Diagrams) method provides high-fidelity database resources to predict stable equilibrium phase assemblages, transition temperatures, and thermodynamic properties as a rigorous function of temperature and local multi-component composition.

These foundational calculations rely on the numerical minimization of a system's total Gibbs free energy under fixed temperature, pressure, and mass balance constraints [5]. While alternative formulations have extended equilibrium calculations to other physical potentials [5], Gibbs energy minimization remains the standard. However, as metallurgical exploration shifts aggressively toward highly complex spaces—such as advanced high-strength steels [6, 7], multi-component superalloys [8], and high-entropy alloys [9]—computational alloy design is confronted by a massive combinatorial explosion of composition variables. Iterative equilibrium solvers are computationally intensive, often requiring several seconds to converge a single design coordinate [10]. When screening millions of potential chemistry combinations in high-dimensional composition spaces, the cumulative computational cost of raw CALPHAD queries becomes prohibitive at screening scale [9, 10].

To circumvent the bottlenecks inherent to iterative thermodynamic solvers, machine-learning (ML) surrogate models are increasingly deployed to replace raw CALPHAD queries [11]. These surrogates—ranging from tabular-oriented ensemble decision trees like Random Forests and XGBoost to deep neural networks (DNNs)—execute rapid forward passes that can provide computational speedups of several orders of magnitude. Such acceleration enables the high-throughput screening of vast, multi-million composition databases in minutes rather than months [11].

Despite these clear performance advantages, predicting multi-phase equilibria directly introduces a unique mathematical challenge: the predicted vector of equilibrium phase fractions must strictly reside on the probability simplex. To satisfy fundamental mass conservation laws, the phase fractions (Nk) for K possible phases must sum to exactly one and remain strictly non-negative [13]:

k=1KNk=1, Nk≥0 (1)

Predictions that violate these structural constraints are physically inadmissible for downstream multiscale models, including kinetic simulations or phase-field modeling [14].

In adjacent fields like geochemistry [15] and agronomy [16], this challenge is addressed through Compositional Data Analysis (CoDA) using log-ratio transformations. In materials informatics, however, the literature exhibits a critical lack of consensus on how to best enforce these physical constraints on neural-network outputs [10]. Some researchers integrate standard softmax layers into multi-phase DNN regressors to natively restrict predictions to a sum of one [10, 13]. Others propose differentiable algorithms, such as DISCOMAX, which utilize straight-through softmax relaxations to guarantee thermodynamic consistency [14].

Conversely, recent deep-learning workflows focusing on complex superalloys found that enforcing a strict 100% sum rule on output heads actually reduced overall predictive accuracy. Consequently, those models defaulted to unconstrained linear outputs, deliberately accepting mass-balance errors to preserve continuous regression performance [8]. Alternative constraint configurations—such as post-hoc renormalization, sparsity-inducing operators like sparsemax, or algebraic residue closure—have been proposed, but their relative tradeoffs regarding predictive accuracy, physical admissibility, and training stability remain unbenchmarked in multi-phase metallurgical settings [14].

A secondary challenge in materials informatics is the evaluation of models beyond standard random or cluster-stratified cross-validation splits [18, 19]. Conventional protocols primarily assess interpolation ability, where queried test points are surrounded by local training neighbors [20]. Practical alloy discovery, however, frequently requires querying entirely unprobed chemical spaces. This introduces complex spatial generalization challenges: predictions must be made either in contiguous, missing interior regions or under strict out-of-range extrapolation [20, 21].

Evaluating surrogate models under these geometric distribution shifts is confounded by data volume. Removing a specific spatial region to construct a validation task inherently removes training data, making it statistically difficult to isolate the true algorithmic penalty of the spatial shift from the penalty of learning from a reduced dataset. Thus, establishing rigorous spatial generalization protocols utilizing size-matched random controls is mathematically necessary to decouple true spatial shifts from mere data-volume effects.

Furthermore, the architectural behavior of ML algorithms under these geometric shifts is starkly distinct. Tabular-oriented algorithms, such as Random Forests, interpolate systems dominated by sharp, binary phase boundaries well, but their step-function decision boundaries prevent them from predicting continuous trends beyond known ranges [4]. DNNs can produce smoother outputs that generalize more gracefully [4, 22]. Despite this potential, recent studies analyzing over 700 out-of-distribution (OOD) tasks demonstrate that true extrapolation beyond the training domain severely degrades predictive fidelity across all standard architectures [20]. To mitigate these limits, researchers have explored transductive approaches [21] or deep generative flow-based imputers [23]. However, a systematic, decoupled evaluation of spatial generalization limits for direct continuous phase fraction prediction remains absent.

An equally critical, yet often neglected, issue in evaluating CALPHAD surrogates is the regressor–detector gap. Standard validation almost exclusively relies on aggregate regression metrics, such as Mean Absolute Error (MAE) [25]. Because zero-fraction rows mathematically dominate global loss calculations in multi-phase databases, an unconstrained model can achieve a deceptively low aggregate error by predicting near-zero fractions for inactive phases, while entirely failing to accurately resolve the emergence of newly stabilizing, rare phases.

In physical metallurgy, this specific modeling failure has severe real-world consequences. Detrimental intermetallic phases—such as the highly embrittling σ-phase in stainless steels—exercise a disproportionate influence on the alloy's mechanical toughness and corrosion properties despite small volume fractions [7, 26]. From a machine-learning perspective, standard uniform loss functions do not penalize their misprediction heavily enough to force gradient descent to learn their distinct, narrow thermodynamic boundaries. Consequently, a surrogate minimizing aggregate regression error is not necessarily an optimal phase-presence detector. This gap is robust across classification thresholds, and discrete phase-presence detection capability degrades much faster than continuous regression error under spatial distribution shifts. Resolving this gap is important for building engineering trust in ML surrogates.

To address these interconnected challenges, this study systematically investigates how neural network architectures can reliably predict multi-phase equilibria while strictly satisfying physical mass conservation. Based on a dataset of 44,397 validated thermodynamic equilibria generated via a probe-driven phase-set pre-screening of five Fe-based ternary systems (Fe–Cr–Ni, Fe–Cr–Mn, Fe–Cr–Mo, Fe–Cr–V, Fe–Mn–Ni), we evaluate the limits of deep learning surrogates under controlled distribution shifts. These benchmark systems cover highly relevant metallurgical phases, including the industrially vital FCC solid-solution structures found in stainless steels and nickel-based superalloys.

The study is deliberately scoped to ternary systems, where ground-truth generation is inexpensive (a few CPU-hours per system), so that every protocol decision can be validated exhaustively; the methodological questions it isolates—constraint enforcement, generalization protocols, and detection—arise identically in the higher-dimensional design spaces where surrogate speed becomes a practical necessity.

The specific contributions of this work are fourfold: First, we benchmark six distinct neural network output configurations against four classical baselines to assess how structural outputs affect both continuous regression accuracy and physical admissibility. Second, we establish decoupled spatial generalization protocols—a contiguous interior-band holdout and a strict one-sided extrapolation task—utilizing size-matched random controls and a region-matched reanalysis to separate spatial penalties from data-volume reductions. Third, we characterize the regressor–detector gap by analyzing a stable discrepancy between continuous regression error and discrete phase-presence detection under distribution shifts. Finally, we provide detailed reporting of informative negative results for three constraint mechanisms to establish clear design guidelines and prevent redundant algorithmic development in future ICME workflows.

# Methods

Figure 1 summarises the pipeline end to end: the CALPHAD data generation, the fixed-protocol split and model families, and the three evaluation protocols they are subjected to.

Figure 1. Study pipeline. (1) CALPHAD data generation: five Fe-based ternary subsystems are extracted from the open MatCalc steel database, probe-driven phase sets fix the target dimensionality, structured sampling draws 11,220 raw design points per system (8,880 of which fall inside the valid sub-simplex and are submitted to the solver), and the equilibrium convergence and mass-balance gate accepts 44,397 equilibria in total. (2) A cluster-stratified 64/16/20 split feeds a constrained MLP with six output heads (plus two mechanism probes) and four classical baselines, all fitted under one fixed protocol and three seeds. (3) Three evaluation protocols − interpolation, contiguous interior-band holdout, and strict one-sided extrapolation, the two spatial ones each with a size-matched random control — plus two secondary analyses (ablations and boundary-error analysis, dashed arrows).

## Data Generation

### Thermodynamic Description

All thermodynamic equilibrium calculations were driven by the open MatCalc steel database (mc_fe_v2.062). To ensure computational compatibility, a custom lenient parser was integrated with pycalphad to extract the relevant five ternary subsystems (Fe–Cr–Ni, Fe–Cr–Mn, Fe–Cr–Mo, Fe–Cr–V, and Fe–Mn–Ni) and implement minor syntax corrections. A rigorous validation step was performed on a pruned version of the database; this verified strict equivalence with the unpruned source, ensuring maximum deviations in phase fractions and Gibbs free energies remained strictly at zero across all systems. For all generated equilibria, the system pressure was fixed at 101,325 Pa.

### Probe-driven Phase Sets

Running complete equilibrium calculations with all eligible phases is computationally intensive, averaging roughly 2.5 seconds per query point. To streamline dataset generation, a phase-set pre-screening was employed. Each of the five systems was independently sampled using 2,000 Dirichlet draws to identify which phases were actively present. As detailed in Table 1, only phases observed to be active during this probing phase were retained as regression targets, reducing the dimensionality (K) from the total eligible phases. This global preprocessing step fixed the output dimensionality for each system prior to any predictive modeling. The fidelity of this phase-set reduction was validated on an independent set of 1,500 points per system by re-solving every point with the complete eligible phase set (25–31 phases depending on system) and comparing per-phase amounts and total molar Gibbs energies against the stored values. In four of the five systems the reduced-set and full-set equilibria agree to solver precision: max |ΔNP| ≤ 2.5 × 10⁻⁹ and max |ΔG| ≤ 7.8 × 10⁻⁵ J/mol, and no excluded phase appears at any sampled point. Fe–Cr–Mo is the exception: at 3 of 1,500 points (0.2%), all located in the Mo-rich, low-temperature corner (x_Mo ≥ 0.42, T ≈ 700 K) where BCC, μ, and Laves phases compete closely, the full-set solve returns a different assemblage involving LAVES_PHASE at up to |ΔNP| = 0.71 and |ΔG| = 6.3 × 10² J/mol. Every phase involved in either solution is already in the probe-active target set, so these discrepancies reflect near-degenerate solver minima in this region rather than an incomplete target set: repeated full-set solves can return either minimum, and the exact failing-point count varies between validation runs (1–3 of 1,500); no excluded phase exceeds the 10⁻³ threshold anywhere.
      |kyk-1|≤3.3×10-8

Phases stable in multiple composition sets (for example the BCC α/α′ miscibility gap) are summed over their composition-set vertices into a single fraction column, matching the vertex accumulation performed by the equilibrium solver. The pre-screening probe and the structured design are different distributions over the Gibbs triangle: the probe retains any phase observed at least once under uniform Dirichlet draws, which is why MNNI2—active in only 0.1% of probe draws and never in the structured design—enters the Fe–Mn–Ni target vector with zero active rows. A phase stable in less than roughly 0.05% of the design space could evade both the 2,000-draw probe and the structured sampling and thus be absent from the closed target basis.

Table 1. Summary of the investigated ternary systems, contrasting the total number of theoretically eligible phases against the verified probe-active target phases (K) utilized as regression targets in this study.

| System | x₂, x₃ | Eligible | K | Target phases |
| --- | --- | --- | --- | --- |
| Fe–Cr–Ni | Cr, Ni | 28 | 4 | BCC_A2, FCC_A1, LIQUID, SIGMA |
| Fe–Cr–Mn | Cr, Mn | 31 | 7 | ALPHA_MN, BCC_A2, BETA_MN, CR3MN5, FCC_A1, LIQUID, SIGMA |
| Fe–Cr–Mo | Cr, Mo | 29 | 9 | BCC_A2, CHI_A12, FCC_A1, LAVES_PHASE, LIQUID, MU_PHASE, MU_PHASE_I, R_PHASE, SIGMA |
| Fe–Cr–V | Cr, V | 25 | 4 | BCC_A2, FCC_A1, LIQUID, SIGMA |
| Fe–Mn–Ni | Mn, Ni | 29 | 7 | ALPHA_MN, BCC_A2, BETA_MN, FCC_A1, LIQUID, MNNI, MNNI2 |

### Sampling and Acceptance

The design variables for each system comprised two independent mole fractions (x2 and x3), with iron serving as the balance element (xFe=1-x2-x3), and temperature (T) sampled uniformly across the 700 to 2000 K domain. To prevent the systematic undersampling of metallurgically critical regions, five deterministic sampling strategies were combined to generate 11,220 raw design points per system. This approach deliberately over-represented the iron-rich corner, isothermal slices, the liquidus zone, and sigma-phase fields. A candidate data point was only incorporated into the final dataset if its composition resided within the defined sub-simplex and its computed equilibrium satisfied a stringent mass-balance tolerance (). Of the 11,220 raw design draws per system, 2,340 fell outside the sub-simplex and were discarded before any equilibrium solve; of the remaining 8,880 valid candidates, 8,877 to 8,880 converged and satisfied mass balance, the only solver rejections being three non-converged points in Fe–Cr–Mo. The 11,220 to 8,880 reduction is therefore a design-space filter rather than a convergence filter, and the datasets contain no solver-driven holes.|kNk-1|<10-6 This acceptance protocol yielded datasets of 8,880 convergent rows per ternary system (8,877 in Fe–Cr–Mo), the statistical compositions of which are summarized in Table 2. The spatial distribution, phase occurrences, and structural closure bounds of this generated data are further visualized in Figure 2.

Table 2. Summary statistics of the generated datasets across the five Fe-based ternary systems, detailing phase occurrence boundaries and maximum deviations in mass-balance simplex closure. Box (%) is the fraction of rows inside the industrially relevant stainless-steel composition box (Fe ≥ 55 at.%, Cr ≤ 30 at.%, X ≤ 30 at.%, with X the third element of the system).

| System | Rows | Box (%) | max¦Σy−1¦ | K | Occurrence range (%) |
| --- | --- | --- | --- | --- | --- |
| Fe–Cr–Ni | 8,880 | 38.0 | 9.8×10⁻⁹ | 4 | 11.94–73.6 |
| Fe–Cr–Mn | 8,880 | 38.0 | 1.2×10⁻⁸ | 7 | 0.03–57.5 |
| Fe–Cr–Mo | 8,877 | 38.0 | 3.3×10⁻⁸ | 9 | 0.10–63.5 |
| Fe–Cr–V | 8,880 | 38.0 | 1.9×10⁻⁸ | 4 | 2.04–79.9 |
| Fe–Mn–Ni | 8,880 | 38.0 | 1.9×10⁻⁹ | 7 | 0.00–76.0 |

Figure 2. Statistical overview of the generated datasets, with a detailed spatial visualization of the Fe–Cr–Ni system. (a) Design points in the composition plane colored by temperature. (b) Marginal density of sampled temperatures. (c) Demarcation of the industrially relevant stainless-steel subset. (d) Logarithmic frequency of target phase occurrences across all five systems. (e) Verification of mass-balance closure for target vectors prior to model training.

## Models and Training

### Neural-Network Architectures and Simplex Constraints

The core predictive model was a multilayer perceptron (MLP) featuring three hidden layers composed of 192 units each, integrated with LayerNorm, SiLU activations, and dropout regularization. Networks were trained via the AdamW optimizer employing cosine annealing, early stopping, and a Huber loss function (Δ=0.01). Features were standardized using scalers fitted to the training partitions only.

To assess the enforcement of the mass-balance constraint (Eq. 1), six distinct output heads were benchmarked:

- An unconstrained sigmoid baseline.

- A standard softmax projection.

- A train-time sigmoid/Σ normalization.

- A renorm head: an independently trained sigmoid model whose outputs are projected at inference time only (clipped to [0, 1], then divided by the row sum). The projection lies outside the training graph, and clipping is active only for baseline outputs that can leave [0, 1], since sigmoid outputs already lie in (0, 1).

- A sparsemax operator designed to produce exact zeros for absent phases.

- A residue closure head that algebraically infers the final phase fraction to enforce sum-to-one equality. Crucially, these models were evaluated not just for closure (summing to one) but for strict simplex membership (closure combined with strict non-negativity across all phase components).

A seventh head, power normalisation (each sigmoid output raised to a power p = 2 and renormalised by its row sum, applied inside the training graph), was evaluated on the Fe–Cr–Ni system only and is marked † in Table 3.

### Baseline Models

To contextualize the neural network performance, four classical machine learning baselines were evaluated: ridge regression, distance-weighted k-nearest neighbors (k=10), XGBoost, and random forests. Because classical regressors do not intrinsically respect structural simplex constraints, each baseline was evaluated both in its raw predictive state and following post-hoc renormalization to yield physically admissible outputs.

### Splitting Protocols and Evaluation Metrics

For standard interpolation evaluations, data points were divided using a cluster-stratified KMeans split (k=6) to generate representative training (64%), validation (16%), and testing (20%) sets across the three-dimensional feature space. To account for stochastic training variance, all experiments were averaged over three distinct random initialization seeds. The K-means stratification, the per-cluster shuffle, and hence the split itself are re-drawn for every seed, so the reported seed-to-seed spread reflects both split variation and training stochasticity. The primary continuous evaluation metric was the mean absolute error (MAE) computed across all phases. Phase-presence detection capabilities were additionally quantified using F1 scores and balanced accuracy, treating any phase with a predicted fractional presence exceeding 10-3 as physically active; the reported mean F₁ is a macro-average over the K phases of each system. All reported metrics are computed on the test partition, which played no role in training or early stopping. A phase with no active row in a given test set (MNNI2, with zero active rows in the whole Fe–Mn–Ni dataset) has an undefined F1; we score it as F1 = 0 for every model, which keeps the phase in the average without favoring any model. Table 6 additionally reports an entropy-weighted MAE, an auxiliary metric intended to up-weight multi-phase coexistence states, where several nonzero phase fractions must be predicted simultaneously; it is an evaluation aid, not a theoretically privileged loss.

## Spatial Generalization Evaluation Protocols

To explicitly test the spatial generalization and extrapolation limits of the surrogate models, two customized data splitting protocols were devised and executed in addition to the standard interpolation split:

- Contiguous Interior-Band Holdout: This protocol removed a specific temperature band (1200–1400 K) and a composition band (x2∈0.25,0.35) entirely from the training data. Delaunay triangulation confirmed that 99.3–99.4% of these held-out points remained within the convex hull of the surrounding training data, framing this as an in-hull distribution shift rather than strict extrapolation.

- Strict One-Sided Extrapolation: To test true out-of-range predictive capacity, models were trained exclusively on one side of a coordinate boundary (e.g., x2≤0.25) and tested strictly on the unobserved far side (e.g., x2>0.35).

A fundamental challenge in measuring spatial generalization is that removing a geometric region concurrently reduces the sheer volume of available training data. To deconvolve the spatial penalty from this data-volume penalty, both spatial protocols were evaluated alongside strictly sized-matched random controls. In these controls, an equivalent number of training rows were randomly excised across the entire domain, and the evaluation is performed on those random rows. The controls therefore ask whether removing a contiguous band is costlier than removing the same number of random rows, but because the control rows differ from the band rows, their ratios conflate region difficulty with distribution shift. As a complementary reference we also report a region-matched reanalysis: for each band, the band-holdout error is compared with the error of the main-study models on the same band rows inside the interpolation test set, where band data were present in training. This ratio isolates the regional shift on identical rows; its residual confound is a training-set size difference of roughly 15%, since removing a band also removes those rows from training.

# Results

## Predictive Accuracy on the Interpolation Split

The primary predictive performance of the evaluated surrogate models on the standard interpolation test sets is summarized in Table 3 and visualized in Figure 3. The comparative analysis reveals that no single architecture universally dominates across the five tested ternary systems. Instead, model performance is strongly correlated with the underlying topological features of each phase diagram.

Constrained multilayer perceptrons (MLPs) demonstrated superior performance on systems characterized by extended, smooth multiphase coexistence fields. For the Fe–Cr–Ni system, the constrained renorm MLP achieved a mean absolute error (MAE) of 0.0106 ± 0.0006, significantly outperforming the random forest baseline (0.0180 ± 0.0002), representing a 41% reduction in error. A similar advantage was observed in the Fe–Cr–Mn system utilizing the sigmoid/Σ head. Conversely, tree-based models were more accurate in systems dominated by sharp, essentially binary phase boundaries. In the Fe–Mn–Ni system, the random forest achieved an MAE of 0.0058 ± 0.0003, outperforming the best constrained MLP (0.0140 ± 0.0013). The Fe–Cr–Mo and Fe–Cr–V systems resulted in statistical ties between the two modeling paradigms, formally confirmed via paired bootstrap resampling over 10,000 iterations (Table 4).

Furthermore, the application of post-hoc renormalization to classical baseline models did not degrade predictive accuracy in any of the five evaluated systems; in fact, the projection reliably recovered valid states and marginally improved the error metrics.

Aggregate cell-averaged MAE also understates worst-case behaviour. Restricting error to active cells (true fraction above 0.005) raises the renorm MLP's MAE from 0.006–0.016 to 0.023–0.074 depending on system (random forest: 0.025–0.049), the 95th percentile of the per-row mean error reaches 0.03–0.12, and the single worst cell in every system is a complete miss (error near 1). Physical admissibility is, moreover, stricter than simplex membership: in a ternary at fixed pressure, more than three phases can coexist only at invariant points, so any prediction assigning more than three phases above the 10⁻³ presence threshold is physically inadmissible. The ground truth contains no such rows, the renorm MLP emits none in four systems (3.4% of Fe–Cr–Mo rows), and the random forest reaches 0–8.9%; XGBoost is the worst offender at up to 22.4% in Fe–Cr–Mo. Simplex-valid outputs therefore do not guarantee phase-rule admissibility, and this axis should accompany closure in future evaluation protocols.

Table 3. Interpolation test MAE across the five ternary systems, averaged over three random initialization seeds. Neural network heads are categorized by their structural adherence to the simplex constraint. Standard deviations are provided in the least significant digits.

| Group | Model | Fe–Cr–Ni | Fe–Cr–Mn | Fe–Cr–Mo | Fe–Cr–V | Fe–Mn–Ni |
| --- | --- | --- | --- | --- | --- | --- |
| off-simplex | sigmoid (unconstrained) | 0.0232 (10) | 0.0163 (1) | 0.0184 (5) | 0.0287 (4) | 0.0231 (13) |
| off-simplex | residue, y(d) = 1−Σ | 0.0229 (3) | 0.0186 (4) | 0.0182 (5) | 0.0254 (3) | 0.0210 (12) |
| on-simplex | sparsemax | 0.0444 (229) | 0.0212 (177) | 0.0573 (427) | 0.0304 (161) | 0.0375 (295) |
| on-simplex | softmax | 0.0130 (3) | 0.0088 (11) | 0.0148 (1) | 0.0167 (2) | 0.0145 (15) |
| on-simplex | sigmoid/Σ (train-time) | 0.0112 (10) | 0.0074 (2) | 0.0126 (2) | 0.0153 (4) | 0.0145 (20) |
| on-simplex | sigmoid + renorm (post hoc) | 0.0106 (6) | 0.0081 (4) | 0.0159 (3) | 0.0149 (4) | 0.0140 (13) |
| on-simplex | power-normalisation (†) | 0.0123 (14) | — | — | — | — |
| baselines | ridge | 0.2053 (9) | 0.1399 (5) | 0.1244 (6) | 0.1940 (8) | 0.0769 (5) |
| baselines | k-NN, k = 10 | 0.0256 (6) | 0.0171 (5) | 0.0151 (6) | 0.0222 (5) | 0.0091 (6) |
| baselines | XGBoost | 0.0212 (6) | 0.0154 (8) | 0.0137 (2) | 0.0179 (3) | 0.0081 (3) |
| baselines | random forest | 0.0180 (2) | 0.0133 (5) | 0.0123 (2) | 0.0137 (4) | 0.0058 (3) |

Table 4. Paired bootstrap statistical comparison of row-wise MAE differences between the best-performing constrained MLP and the random forest baseline on the interpolation test set (95% confidence interval, 10,000 resamples).

| System | Best MLP head | ΔMAE (MLP−RF) | 95% CI | Verdict |
| --- | --- | --- | --- | --- |
| Fe–Cr–Ni | renorm | -0.00737 | [-0.00850, -0.00627] | MLP better |
| Fe–Cr–Mn | sig-norm | -0.00593 | [-0.00670, -0.00514] | MLP better |
| Fe–Cr–Mo | sig-norm | +0.00027 | [-0.00054, +0.00109] | tie |
| Fe–Cr–V | renorm | +0.00115 | [-0.00071, +0.00303] | tie |
| Fe–Mn–Ni | renorm | +0.00821 | [+0.00678, +0.00970] | RF better |

Figure 3. Comparative regression accuracy and constraint adherence. (a) Mean test MAE for the evaluated neural network heads. (b) Relative MAE performance ratio of the best constrained MLP against the random forest baseline. (c) Quantification of simplex closure violations, demonstrating that structurally constrained heads and renormalized baselines satisfy mass-balance within machine precision bounds.

## Mass-Balance Simplex Closure

Enforcing the physical mass-balance requirement is critical for the admissibility of surrogate outputs in subsequent thermodynamic calculations. As detailed in Table 5, all structurally constrained neural network heads satisfied the closure equality constraint (kyk=1) to within 32-bit floating-point precision (≤5×10-8). In stark contrast, unconstrained sigmoid outputs violated this fundamental closure requirement by an average of 6% to 8%, and raw tree-based outputs exhibited violations between 0.9% and 4.7%. While post-hoc renormalization successfully repaired baseline outputs to machine precision (∼10-17), the structurally constrained MLPs achieved this physically admissible state natively without requiring secondary projection steps.

Table 5. Mean closure violations (|kyk-1|) on the test partition. Structurally constrained architectures achieve closure at float32 precision, while unconstrained models exhibit unphysical deviations spanning orders of magnitude.

| Closure | Model | Fe–Cr–Ni | Fe–Cr–Mn | Fe–Cr–Mo | Fe–Cr–V | Fe–Mn–Ni |
| --- | --- | --- | --- | --- | --- | --- |
| none | sigmoid | 6.2×10⁻² | 8.1×10⁻² | 8.1×10⁻² | 6.3×10⁻² | 7.4×10⁻² |
| none | random forest, raw | 2.8×10⁻² | 2.9×10⁻² | 4.7×10⁻² | 1.5×10⁻² | 8.7×10⁻³ |
| none | XGBoost, raw | 2.8×10⁻² | 3.3×10⁻² | 4.1×10⁻² | 2.1×10⁻² | 1.6×10⁻² |
| structural | softmax | 3.3×10⁻⁸ | 4.8×10⁻⁸ | 4.4×10⁻⁸ | 3.4×10⁻⁸ | 4.5×10⁻⁸ |
| structural | sigmoid/Σ | 1.7×10⁻⁸ | 2.7×10⁻⁸ | 3.3×10⁻⁸ | 1.6×10⁻⁸ | 3.1×10⁻⁸ |
| structural | sparsemax | 1.7×10⁻⁸ | 1.8×10⁻⁸ | 5.0×10⁻⁸ | 1.0×10⁻⁸ | 4.0×10⁻¹⁰ |
| structural | residue | 9.2×10⁻⁹ | 1.9×10⁻⁸ | 1.8×10⁻⁸ | 6.5×10⁻⁹ | 1.8×10⁻⁸ |
| post hoc | sigmoid + renorm | 1.5×10⁻⁸ | 2.5×10⁻⁸ | 2.5×10⁻⁸ | 1.2×10⁻⁸ | 3.3×10⁻⁸ |
| post hoc | random forest + renorm | 2.3×10⁻¹⁷ | 2.0×10⁻¹⁷ | 3.8×10⁻¹⁷ | 1.5×10⁻¹⁷ | 8.9×10⁻¹⁸ |

## The Regressor–Detector Gap

A critical distinction emerged between continuous regression accuracy (MAE) and discrete phase-presence detection (quantified via F₁ scores and balanced accuracy). As summarized in Table 6 and Figure 4, the model minimizing aggregate MAE is not necessarily the optimal phase-presence detector. This discrepancy is largely attributed to the sparsity of rare phases: zero-fraction rows dominate the global loss calculation, meaning a model can achieve a low aggregate MAE while entirely failing to resolve a trace phase. For example, in the Fe–Mn–Ni system, the MLP failed to detect three rare phases (F₁ = 0), whereas the random forest successfully resolved two of them. This gap is not an artefact of the zero-positive scoring convention: excluding zero-positive phases from the macro-average raises the Fe–Mn–Ni MLP F₁ only from 0.312 to 0.364, versus 0.504 to 0.588 for the random forest. Threshold-free per-phase average precision (AUPRC) confirms the pattern: across the ten rare phases with occurrence below 5%, the renorm MLP's average precision is 0.001–0.05 for nine of them (for example 0.014 for the 2%-occurrence FCC phase in Fe–Cr–V and 0.003 for MNNI in Fe–Mn–Ni; the exception is FCC in Fe–Cr–Mo at 0.63), whereas the random forest retains 0.40–0.97 in all of them except the two near-zero-occurrence phases (CR3MN5 at 0.03% and MU_PHASE_I at 0.1%), where both families fail.

This regressor–detector gap proved robust across varying classification thresholds. Sensitivity analyses evaluating phase presence thresholds of 10⁻⁴, 10⁻³, and 10⁻² (Table 7) confirmed that while absolute F₁ scores shifted as expected, the relative rank order of model detection capability remained highly stable across four of the five systems. Crucially, phase-presence detection degrades under the spatial holdouts: on the held-out temperature bands, macro-F₁ falls by roughly 20–60% in relative terms in all five systems and for both model families (for example, the Fe–Cr–Ni MLP falls from 0.93 to 0.64 and its random forest from 0.85 to 0.53, even as regression MAE remains comparatively stable), whereas the composition bands affect detection more mildly for the MLP (2–10% relative) than for the random forest (7–44%).

Table 6. Quantitative comparison of continuous regression performance (MAE) versus discrete phase-presence detection (F₁ score and balanced accuracy). The data highlight that optimal regression performance does not inherently guarantee optimal phase detection.

| System | Model | MAE | F₁ | Bal. acc. | Entropy-w. MAE |
| --- | --- | --- | --- | --- | --- |
| Fe–Cr–Ni | MLP renorm | 0.0106 | 0.927 | 0.939 | 0.0137 |
|  | random forest | 0.0180 | 0.846 | 0.887 | 0.0218 |
| Fe–Cr–Mn | MLP sig-norm | 0.0074 | 0.527 | 0.752 | 0.0089 |
|  | random forest | 0.0133 | 0.592 | 0.850 | 0.0150 |
| Fe–Cr–Mo | MLP sig-norm | 0.0126 | 0.643 | 0.827 | 0.0149 |
|  | random forest | 0.0123 | 0.629 | 0.858 | 0.0147 |
| Fe–Cr–V | MLP renorm | 0.0149 | 0.718 | 0.822 | 0.0167 |
|  | random forest | 0.0137 | 0.785 | 0.893 | 0.0158 |
| Fe–Mn–Ni | MLP renorm | 0.0140 | 0.312 | 0.643 | 0.0158 |
|  | random forest | 0.0058 | 0.504 | 0.884 | 0.0063 |

Table 7. Sensitivity analysis of phase-presence detection metrics as a function of the minimum fractional presence threshold, confirming the stability of the observed regressor–detector gap.

| System | Model | F₁ at 10⁻⁴ | F₁ at 10⁻³ | F₁ at 10⁻² |
| --- | --- | --- | --- | --- |
| Fe–Cr–Ni | best MLP (renorm) | 0.870 (6) | 0.927 (4) | 0.962 (3) |
|  | random forest | 0.815 (6) | 0.846 (6) | 0.911 (2) |
| Fe–Cr–Mn | best MLP (sig-norm) | 0.489 (6) | 0.527 (2) | 0.550 (2) |
|  | random forest | 0.571 (20) | 0.592 (18) | 0.672 (19) |
| Fe–Cr–Mo | best MLP (sig-norm) | 0.562 (13) | 0.643 (2) | 0.710 (3) |
|  | random forest | 0.590 (2) | 0.629 (3) | 0.727 (4) |
| Fe–Cr–V | best MLP (renorm) | 0.671 (35) | 0.718 (1) | 0.731 (1) |
|  | random forest | 0.767 (6) | 0.785 (9) | 0.870 (6) |
| Fe–Mn–Ni | best MLP (renorm) | 0.306 (5) | 0.312 (4) | 0.314 (4) |
|  | random forest | 0.470 (0) | 0.504 (1) | 0.603 (21) |

Figure 4. Analysis of the regressor–detector gap. (a) Parity plot contrasting the predictive accuracy of the most frequent versus least frequent phases in the Fe–Cr–Ni system. (b) Correlation between per-phase MAE and overall phase occurrence frequency. (c) Ratio comparison of MAE against F₁ score, illustrating domains where optimal regressors act as inferior detectors.

## Spatial Generalization and Extrapolation Limits

The models were subjected to spatial generalization tests utilizing size-matched random controls together with a region-matched reanalysis to separate spatial degradation from training data attrition.

Contiguous Interior-Band Holdout: Results for the missing-region generalization test (Table 8, Figure 5a) require two complementary references. The size-matched random controls ask whether removing a contiguous band is costlier than removing the same number of random rows, but they are evaluated on different, average-difficulty rows and therefore conflate region difficulty with distribution shift. The region-matched reanalysis (Methods) instead compares the same band rows with and without regional training data, and under this measure the picture is consistent: the in-distribution-to-holdout penalty is smaller for the constrained MLPs than for the tree ensembles in nine of the ten band × system combinations. On the composition bands, which cross steep phase boundaries, the MLP penalty ratios are 1.2–2.1 versus 1.4–3.0 for the random forest and XGBoost in all five systems; on the temperature bands the MLP ratios are 0.9–2.8 versus 1.3–3.9, with Fe–Cr–Ni the single exception, where the random-forest ratio is lower (2.1× versus 2.8×) although its absolute holdout error remains twice the MLP's. Ratios must nonetheless be read alongside absolute errors: a band that is easy in distribution, such as the nearly single-phase 1200–1400 K band of Fe–Mn–Ni, inflates ratios through a small denominator.

Strict One-Sided Extrapolation: As detailed in Table 9 and Figure 6, true out-of-range extrapolation yielded severe degradation across all evaluated model families. For compositional extrapolation in the Fe–Cr–Ni system, MAE deteriorated by an order of magnitude, rising to ~0.17 for the constrained MLP and ~0.22 for the random forest, relative to ~0.012 on the matched interpolation controls. The temperature protocol is, however, additionally limited by the closed phase basis: liquid has no active row in the near-side training data (T ≤ 1200 K) in four of the five systems (Fe–Cr–Mo retains some low-temperature liquid), so the far side demands a phase that the target basis cannot express. In Fe–Mn–Ni this renders the task nearly uninformative: all four model families land within 4% of the constant near-side-mean predictor (MAE 0.182–0.184 versus 0.190), and the per-phase errors show that the unseen liquid column alone contributes 0.088 of the 7-phase mean, its entire far-side mean fraction of 0.613 being missed. In the other systems the models still beat the constant predictor substantially (for example 0.099–0.197 in Fe–Cr–V versus 0.307 for the constant predictor), indicating partial transfer of the seen-phase structure. The composition protocol, by contrast, keeps every frequent phase inside the training basis (only trace phases such as ALPHA_MN, BETA_MN, and MNNI on the Mn-rich far side of Fe–Mn–Ni are unseen) and therefore measures genuine spatial extrapolation. Within these protocols the MLP heads achieved the lowest far-side absolute MAE relative to the tree ensembles in all five systems, but the overarching result underscores that no evaluated architecture extrapolates phase fractions reliably beyond the explicit limits of the training domain.

Table 8. Predictive degradation under contiguous interior-band holdouts. Penalty ratios compare the holdout error against a size-matched random control (an equal number of rows removed at random and evaluated on those random rows). This quantifies whether removing a contiguous band is costlier than removing random rows, but does not by itself separate region difficulty from distribution shift; a region-matched reanalysis on identical band rows is reported in the text.

| Held-out region | Model | Fe–Cr–Ni | Fe–Cr–Mn | Fe–Cr–Mo | Fe–Cr–V | Fe–Mn–Ni |
| --- | --- | --- | --- | --- | --- | --- |
| random control | MLP renorm | 0.0101 (8) | 0.0083 (6) | 0.0153 (5) | 0.0234 (70) | 0.0122 (2) |
| random control | MLP sigmoid/Σ | 0.0107 (10) | 0.0077 (6) | 0.0125 (7) | 0.0146 (13) | 0.0123 (1) |
| random control | random forest | 0.0198 (11) | 0.0142 (5) | 0.0140 (11) | 0.0155 (12) | 0.0058 (4) |
| random control | XGBoost | 0.0237 (9) | 0.0167 (6) | 0.0152 (11) | 0.0194 (7) | 0.0084 (1) |
| T ∈ [1200, 1400] K | MLP renorm | 0.0132 (9) | 0.0079 (4) | 0.0266 (4) | 0.0358 (3) | 0.0022 (0) |
| T ∈ [1200, 1400] K | MLP sigmoid/Σ | 0.0144 (32) | 0.0077 (0) | 0.0265 (4) | 0.0372 (12) | 0.0024 (2) |
| T ∈ [1200, 1400] K | random forest | 0.0258 (10) | 0.0123 (2) | 0.0309 (12) | 0.0762 (97) | 0.0090 (6) |
| T ∈ [1200, 1400] K | XGBoost | 0.0408 (17) | 0.0203 (16) | 0.0348 (17) | 0.0823 (77) | 0.0167 (7) |
| x₂ ∈ [0.25, 0.35] | MLP renorm | 0.0162 (7) | 0.0071 (0) | 0.0155 (5) | 0.0111 (52) | 0.0005 (0) |
| x₂ ∈ [0.25, 0.35] | MLP sigmoid/Σ | 0.0163 (6) | 0.0071 (3) | 0.0144 (7) | 0.0075 (15) | 0.0010 (5) |
| x₂ ∈ [0.25, 0.35] | random forest | 0.0615 (73) | 0.0223 (6) | 0.0259 (9) | 0.0288 (5) | 0.0043 (1) |
| x₂ ∈ [0.25, 0.35] | XGBoost | 0.0530 (22) | 0.0250 (11) | 0.0324 (3) | 0.0368 (27) | 0.0063 (7) |
| penalty T / x₂ | MLP renorm | 1.31 / 1.61 | 0.95 / 0.85 | 1.74 / 1.01 | 1.53 / 0.48 | 0.18 / 0.04 |
| penalty T / x₂ | MLP sigmoid/Σ | 1.34 / 1.52 | 1.00 / 0.92 | 2.12 / 1.16 | 2.55 / 0.52 | 0.20 / 0.08 |
| penalty T / x₂ | random forest | 1.31 / 3.11 | 0.86 / 1.57 | 2.21 / 1.85 | 4.92 / 1.86 | 1.54 / 0.73 |
| penalty T / x₂ | XGBoost | 1.72 / 2.24 | 1.21 / 1.49 | 2.29 / 2.13 | 4.24 / 1.89 | 2.00 / 0.75 |

Table 9. Absolute MAE and penalty ratios for strict one-sided extrapolation beyond the established bounds of the training coordinates. All models exhibit sharp error increases under genuine extrapolation. Standard deviations are seed-to-seed; the large-looking Fe–Cr–V random-control deviation (0.0242 ± 0.0073) reflects ordinary seed variability (per-seed values 0.027/0.014/0.031), not a diverged run. The temperature protocol additionally tests an out-of-basis target, as LIQUID is absent from the near-side training data in four of the five systems.

| Region | Model | Fe–Cr–Ni | Fe–Cr–Mn | Fe–Cr–Mo | Fe–Cr–V | Fe–Mn–Ni |
| --- | --- | --- | --- | --- | --- | --- |
| random control (x₂-matched) | MLP renorm | 0.0123 (3) | 0.0094 (2) | 0.0181 (5) | 0.0242 (73) | 0.0135 (6) |
| random control (x₂-matched) | MLP sigmoid/Σ | 0.0128 (16) | 0.0092 (3) | 0.0144 (5) | 0.0163 (13) | 0.0146 (10) |
| random control (x₂-matched) | random forest | 0.0236 (7) | 0.0168 (1) | 0.0167 (6) | 0.0191 (11) | 0.0084 (2) |
| random control (x₂-matched) | XGBoost | 0.0283 (14) | 0.0202 (7) | 0.0184 (5) | 0.0235 (16) | 0.0118 (2) |
| train x₂ ≤ 0.25, test x₂ > 0.35 | MLP renorm | 0.1721 (77) | 0.0458 (17) | 0.0668 (26) | 0.0464 (66) | 0.0143 (25) |
| train x₂ ≤ 0.25, test x₂ > 0.35 | MLP sigmoid/Σ | 0.1709 (65) | 0.0526 (28) | 0.0689 (8) | 0.0478 (60) | 0.0129 (8) |
| train x₂ ≤ 0.25, test x₂ > 0.35 | random forest | 0.2152 (9) | 0.0788 (5) | 0.1052 (22) | 0.0761 (50) | 0.0279 (6) |
| train x₂ ≤ 0.25, test x₂ > 0.35 | XGBoost | 0.2267 (28) | 0.0860 (47) | 0.1082 (12) | 0.1015 (38) | 0.0329 (3) |
| random control (T-matched) | MLP renorm | 0.0127 (2) | 0.0100 (2) | 0.0187 (8) | 0.0277 (4) | 0.0142 (5) |
| random control (T-matched) | MLP sigmoid/Σ | 0.0142 (12) | 0.0102 (3) | 0.0153 (4) | 0.0158 (8) | 0.0151 (4) |
| random control (T-matched) | random forest | 0.0245 (10) | 0.0178 (5) | 0.0173 (6) | 0.0194 (17) | 0.0080 (3) |
| random control (T-matched) | XGBoost | 0.0285 (14) | 0.0214 (3) | 0.0191 (5) | 0.0243 (18) | 0.0111 (1) |
| train T ≤ 1200 K, test T > 1400 K | MLP renorm | 0.2227 (66) | 0.1262 (41) | 0.0823 (27) | 0.0994 (6) | 0.1823 (0) |
| train T ≤ 1200 K, test T > 1400 K | MLP sigmoid/Σ | 0.2241 (96) | 0.1266 (48) | 0.0796 (19) | 0.0991 (11) | 0.1822 (0) |
| train T ≤ 1200 K, test T > 1400 K | random forest | 0.2346 (4) | 0.1524 (13) | 0.1073 (8) | 0.1937 (10) | 0.1834 (1) |
| train T ≤ 1200 K, test T > 1400 K | XGBoost | 0.2327 (6) | 0.1536 (16) | 0.1054 (5) | 0.1972 (20) | 0.1841 (2) |
| penalty x₂ / T | MLP renorm | 13.98 / 17.60 | 4.89 / 12.57 | 3.69 / 4.40 | 1.92 / 3.59 | 1.06 / 12.85 |
| penalty x₂ / T | MLP sigmoid/Σ | 13.36 / 15.78 | 5.74 / 12.46 | 4.78 / 5.19 | 2.93 / 6.25 | 0.88 / 12.05 |
| penalty x₂ / T | random forest | 9.12 / 9.56 | 4.69 / 8.55 | 6.29 / 6.21 | 3.99 / 9.97 | 3.30 / 22.84 |
| penalty x₂ / T | XGBoost | 8.02 / 8.16 | 4.25 / 7.19 | 5.87 / 5.51 | 4.31 / 8.11 | 2.79 / 16.64 |

Figure 5. Generalization degradation analyses. (a) Penalty ratios corresponding to the contiguous interior-band holdouts. (b) Effect of neural network hidden-layer width on predictive accuracy. (c) Sensitivity of the renorm and sigmoid/Σ heads to the selection of the loss function.

Figure 6. Strict one-sided extrapolation evaluation. (a) Penalty ratios for compositional and temperature extrapolation versus size-matched controls. (b) Absolute test MAE values on the extrapolated far side, highlighting the persistent challenge of out-of-support prediction.

## Model Ablations

To dissect the architectural dependencies of the neural network surrogates, a series of ablation studies were performed on the Fe–Cr–Ni system (Table 10, Figures 5b and 5c). The selection of loss function proved highly influential; mean squared error (MSE) exacerbated MAE by 47% relative to Huber (Δ=0.01) or standard MAE losses, primarily because trace phase outliers disproportionately skewed the squared gradient. Increasing hidden-layer capacity from 64 to 256 units monotonically improved accuracy, indicating that the default 192-unit architecture used across the benchmarking suite leaves further optimization headroom. Crucially, attempting to enforce mass balance via a soft sum-to-one loss penalty ( and ) degraded the overall fit by a factor of 8 to 16 without achieving the numerical strictness provided by structural output constraints. The penalty weights were restricted to λ ∈ {1, 10}: with the Huber regression term saturating its per-output gradient at δ = 0.01, these weights make the closure term dominate the regression gradient by one to two orders of magnitude, and no smaller λ, gradient-rescaled penalty, or warm-up schedule was evaluated. The defensible conclusion is therefore that the soft penalty adds nothing over the structural heads at the tested weights, not that soft penalties are unviable in general.λ=1
      λ=10

Table 10. Architectural ablation study for the Fe–Cr–Ni system, evaluating the impacts of loss function formulation, network capacity, and soft closure penalties on the interpolation MAE.

| Ablation | Setting | renorm | sigmoid/Σ |
| --- | --- | --- | --- |
| loss | Huber, δ = 0.01 (default) | 0.0106 (6) | 0.0112 (10) |
| loss | MAE | 0.0103 (6) | 0.0112 (4) |
| loss | MSE | 0.0156 (5) | 0.0152 (6) |
| width | 3×64 | 0.0137 (6) | 0.0139 (10) |
| width | 3×128 | 0.0114 (5) | 0.0131 (17) |
| width | 3×192 (default) | 0.0106 (6) | 0.0112 (10) |
| width | 3×256 | 0.0099 (7) | 0.0105 (7) |
| closure penalty | none | 0.0232 (10), closure 6.2×10⁻² |  |
| closure penalty | λ=1 | 0.0804 (51), closure 2.2×10⁻³ |  |
| closure penalty | λ=10 | 0.1693 (228), closure 1.3×10⁻³ |  |

## Evaluation of Failed Constraint Mechanisms (Negative Results)

Three theoretically plausible physical constraint mechanisms failed under the evaluated configurations (Figure 7), providing critical mechanistic insights into model formulation:

- Sparsemax: While successfully projecting logits to produce exact zeros, this operator exhibited severe seed sensitivity. The resulting inter-seed variance was on the same order of magnitude as the mean MAE, consistent with the hypothesis that gradients vanish identically once a logit drops below the threshold, trapping the network in poor initial local minima.

- Sum-to-One Penalty: As noted in the ablations, enforcing mass balance strictly as a regularizing loss term created pathological competition with the regression targets, buying partial closure entirely at the expense of model fit.

- Residue Closure: The algebraic deduction of the K-th phase fraction (yK=1-k<Kyk) enforces sum-to-one closure by construction but does not intrinsically guarantee non-negativity: if the other predicted fractions sum to more than one, the residue is negative. In the stored predictions, the residue head emitted negative values on 0.0% (Fe–Cr–V), 0.02% (Fe–Mn–Ni), 0.40% (Fe–Cr–Ni), 0.50% (Fe–Cr–Mn), and 1.21% (Fe–Cr–Mo) of cells, with the most negative cell at −0.59. It is therefore closure-valid but not simplex-valid. It was also the least accurate constrained variant: even the best residue head was 1.3–2.5× worse than the best constrained head in the same system, and a sweep over all K choices of the dropped phase (Figure 7c) shows the best choice is the dominant phase in four of five systems. The observed degradation is consistent with the residual phase absorbing the accumulated prediction error of the other K−1 channels; we note this as an interpretation supported by the sweep, not a directly demonstrated mechanism.

Figure 7. Diagnostic overview of failed constraint mechanisms. (a) Severe seed sensitivity and variance observed using the sparsemax operator. (b) The detrimental tradeoff between enforcing a soft closure penalty and maintaining regression accuracy. (c) Error accumulation in the residue closure head as a function of the chosen residual phase.

## Phase Field Visualization and Error Concentration

Qualitative and quantitative assessments of the predicted phase fields (Figure 8) underscore the topological nature of the surrogate errors. Visual analysis of the Fe–Cr–Ni domain under the renorm head confirms that the neural surrogate faithfully reproduces the complex geometry of the underlying CALPHAD phase fields, accurately mapping the BCC, FCC, liquid, and sigma topologies.

However, mapping the spatial distribution of the absolute error reveals significant spatial concentration. By computing the parametric distance of each test row to the nearest shift in the active-phase set, it was determined that mean absolute errors in the closest spatial tertile to a phase boundary averaged 0.022, compared to 0.002 in the most distant interior tertile. This indicates that surrogate uncertainty is highly concentrated directly at structural phase boundaries, whereas the interior of single- or stable multi-phase fields is reproduced with an order of magnitude higher fidelity.

Figure 8. Ground-truth and predicted phase-fraction fields for the Fe–Cr–Ni system evaluated with the renorm head. The absolute error maps highlight the geometric concentration of predictive uncertainty at phase boundaries relative to the stable interiors of phase fields.

# Discussion

## Topological Dependencies and Spatial Concentration of Error

The primary finding from our standard interpolation benchmarking (Table 3, Figure 3) is that the optimal machine learning architecture is not a universal construct; rather, within the five systems evaluated it is strongly shaped by the physical-topological characteristics of the underlying thermodynamic phase diagram [10].

In alloy systems dominated by wide, continuously transitioning multi-phase fields, Deep Neural Networks (DNNs) with smooth, structurally constrained output heads (such as standard softmax or train-time sigmoid/Σ normalization) performed best in two of the five systems [4]. This behavior is prominent in the Fe–Cr–Ni and Fe–Cr–Mn systems, with Fe–Cr–Mo a statistical tie between the families. For example, the Fe–Cr–Ni system features a wide face-centered cubic (FCC) solid-solution matrix transitioning smoothly into body-centered cubic (BCC) and topologically close-packed (TCP) σ intermetallics [27, 28]. The continuous, highly differentiable parameterization of Multilayer Perceptrons (MLPs) naturally aligns with these smooth thermodynamic fraction gradients, allowing the network to regress phase fraction shifts with high fidelity.

Conversely, in alloy systems governed by steep, nearly vertical phase boundaries—such as the sharp FCC-to-liquid boundaries in Fe–Mn–Ni or the abrupt BCC-to-σ transitions in Fe–Cr–V—classical tree-based architectures (such as Random Forests and XGBoost) achieve the best interpolation performance in Fe–Mn–Ni, whereas Fe–Cr–V, another sharp-boundary system, is a statistical tie between the families [4, 29]. The axis-aligned partitioning logic of decision trees is highly efficient at representing step-like, non-differentiable phase boundaries without artificially smoothing the transitions. However, this topological model dependency reveals a severe limitation: tree-based models lack the smooth extrapolation and continuous interpolation capabilities necessary for multi-scale simulations, such as phase-field modeling [30].

Furthermore, irrespective of the chosen model family, predictive uncertainty is geometrically constrained by the phase diagram topology. By mapping the spatial distribution of the absolute error of our surrogate models (Figure 8), we observe that predictive error is not uniformly distributed across the composition–temperature space. Instead, absolute errors are strongly concentrated at the phase boundaries—where the active-phase set changes. Under the best-performing constrained MLP (the renorm head in Fe–Cr–Ni), the mean absolute error (MAE) in the spatial tertile closest to a phase boundary averages 0.022, whereas the stable interiors of single-phase or multi-phase fields are reproduced with errors roughly an order of magnitude lower, averaging 0.002 (an order of magnitude lower). This spatial concentration of error highlights that surrogate model evaluations should move beyond simple global metrics (such as aggregate MAE) to incorporate spatially resolved topological diagnostics (see Figure 8).

## The Reality of Spatial Generalization in Alloy Design

Evaluating machine learning surrogates beyond standard random cross-validation splits is essential for assessing their viability in actual alloy discovery workflows. Random splitting assumes that the test set is independent and identically distributed (i.e., interpolation), but practical alloy design frequently requires navigating "holes" in experimental or computational data, or exploring entirely unprobed chemical spaces [20]. Our spatial generalization protocols explicitly test these out-of-distribution (OOD) boundaries by separating spatial shift penalties from simple data-volume constraints.

Under contiguous, in-hull spatial shifts—simulating missing interior data such as a temperature-band holdout (1200–1400 K) or a composition-band holdout (x₂ ∈ [0.25, 0.35])—MLPs degrade more gracefully than tree-based models. Under the region-matched reanalysis (Methods), the in-distribution-to-holdout penalty on identical band rows is 1.2–2.1 for the constrained MLPs on the composition bands and 0.9–2.8 on the temperature bands, versus 1.3–3.9 for Random Forests and XGBoost, and is smaller for the MLPs in nine of the ten band × system combinations. Tree ensembles partition the input space into piecewise-constant regions; inside a missing band their predictions revert to the constant leaf values of the surrounding partition and change abruptly at partition boundaries, producing step-like predictions. In contrast, the continuous parameterization of MLPs bridges these spatial gaps smoothly, making them more robust for "filling in" missing thermodynamic coordinate spaces under the evaluated band protocols.

However, this graceful in-hull degradation must not be conflated with true thermodynamic extrapolation. When subjected to strict, out-of-range, one-sided extrapolation (e.g., training on x2≤0.25 and testing on x2>0.35, or training on T≤1200 K and testing on T>1400 K), predictive accuracy degrades severely across all evaluated model families. Absolute MAEs on the far side climb to 0.17 to 0.22, representing a 10-to-20-fold degradation compared to matched interpolation controls (Figure 6). Part of the temperature-protocol degradation is a closed-basis limitation rather than a spatial-generalization failure: liquid is absent from the near-side training data in four of the five systems, and in Fe–Mn–Ni all four model families come within 4% of the constant near-side-mean predictor. Extrapolation conclusions should therefore be read as joint failures of basis and generalization. This severe degradation aligns with extensive out-of-distribution materials informatics benchmarks of over 700 OOD tasks, which show that standard deep learning architectures struggle with true extrapolation because the target spaces fall outside their representational support. Merely scaling up dataset size or training time yields diminishing returns in these extrapolative regimes, necessitating alternative transductive architectures that learn relative property changes rather than absolute values, or deep generative flow-based models to "imagine" missing boundaries [23].

## Thermodynamic Fidelity versus Numerical Emulation

To establish a rigorous epistemic foundation for materials informatics, we must distinguish between thermodynamic physical truth and numerical emulation. A machine learning surrogate is not a physical theory; it is strictly a high-speed numerical emulator trained to approximate the outputs of an underlying CALPHAD solver, executing the mapping:

x,T→yCALPHAD

Consequently, the surrogate model intrinsically inherits all underlying thermodynamic assumptions (such as global equilibrium postulates) and databases (such as MatCalc mc_fe_v2.062) used to generate the training data. High accuracy on a test partition simply confirms that the neural network has successfully emulated the solver's numerical optimization to float32 precision. It does not validate the physical accuracy of the CALPHAD model itself. For example, if a CALPHAD database fails to capture a metastable phase due to a lack of assessed binary or ternary interaction parameters [8], the surrogate will mathematically replicate this blind spot.

This distinction emphasizes the role of surrogates as high-speed screening filters rather than thermodynamic arbiters. While the 104-fold speedups provided by MLPs enable the screening of multi-million composition databases in seconds, any candidate alloy identified during high-throughput screening must be independently re-validated using direct CALPHAD calculations and, ultimately, targeted experimental synthesis. Measured on CPU, the 192-unit MLP forward pass costs 2–3 µs per point in batch inference (0.4–0.6 ms for a single query), against roughly 2.5 s per equilibrium on the CALPHAD side of this work — a speedup of about 10⁶ in batch mode and 4–6 × 10³ for single queries.

## The Metallurgy of the Regressor–Detector Gap

A critical, often neglected issue in materials informatics is the "regressor–detector gap," where models optimized for continuous regression (lowest overall MAE) act as poor phase-presence detectors. In physical metallurgy, minor or rare phases exercise a disproportionate influence on an alloy's properties. For example, the presence of trace intermetallics (such as the embrittling σ-phase in stainless steels) or minor reinforcing carbides can completely alter mechanical strength, creep resistance, and corrosion properties [31, 32].

From a machine-learning perspective, these rare phases are cheap in terms of global loss calculations. Because zero-fraction rows mathematically dominate the multi-phase alloy database (as candidate phases are absent across vast composition–temperature coordinates), a model can achieve a deceptively low aggregate MAE of 0.007 by predicting near-zero fractions for inactive phases, while entirely failing to resolve the stabilizing boundaries of rare, trace, or minor phases.

As detailed in Table 6, this leads to a stable discrepancy: in the Fe–Cr–Mn system, the MLP achieves the lowest continuous regression error yet the random forest is the better detector; in the Fe–Mn–Ni system, the random forest wins both tasks, while the MLP exhibits an exceptionally poor F1 score (0.312) and fails to detect three rare phases entirely (MNNI, MNNI2, and ALPHA_MN). In contrast, the random forest pairs the lowest continuous error in that system with a significantly more robust detector (F1 score of 0.504). This regressor–detector gap is robust across varying classification thresholds (10-4 to 10-2), and more importantly, discrete phase-presence detection degrades faster than continuous regression error under the spatial holdouts evaluated here (macro-F₁ falling by 20–60% in relative terms on the temperature bands, versus MAE penalties of roughly 1–4× on the same bands). This finding suggests that future materials informatics workflows must utilize multi-criteria validation, incorporating classification-based metrics (such as F1 scores and balanced accuracy) alongside continuous regression errors to build reliable surrogates.

## Limitations and Mechanistic Insights from Negative Results

A primary value of this study lies in the detailed characterization of negative results, which establishes clear boundaries and prevents redundant developmental efforts in materials informatics. Three theoretically plausible constraint mechanisms failed under the tested configurations. Sparsemax (Figure 7a) exhibited severe seed-to-seed variance, consistent with gradients vanishing once a logit is projected to zero; notably, it was trained with a regression loss on its projected outputs—the configuration most exposed to that zero-gradient region—so the dedicated sparsemax loss and α-entmax variants remain untested. The soft sum-to-one penalty (Figure 7b) degraded the fit by a factor of 8–16 at the tested weights, which dominate the Huber regression gradient by one to two orders of magnitude; smaller weights or rescaled penalties were not evaluated. The residue closure head (Figure 7c) accumulated the prediction error of the other channels into a single unconstrained output and frequently produced negative fractions. These are scoped conclusions about the tested configurations, not about the mechanisms in principle; the mechanistic details and per-phase diagnostics are reported in the Results.

Several protocol-level caveats bound the generality of these findings. The contiguous-band holdout is a missing-region test inside the sampled domain, and the strict extrapolation protocol is one-sided, covering only one coordinate at a time; behavior beyond the sampled simplex remains unvalidated. The design distribution is deliberately structured, not uniform, so all reported average errors are expectations under that sampling distribution, and rankings could shift under a different prior. All MLPs share one fixed architecture and all baselines use fixed hyperparameters: the comparison is a fixed-protocol benchmark, not an exhaustive hyperparameter search, and the reported MLP is not architecture-optimal. The mean ± standard deviation over three seeds quantifies seed-to-seed training stochasticity only, not total predictive uncertainty. The phase-boundary analysis uses an empirical boundary proxy — the distance to the nearest sampled row with a different active-phase set — not the exact thermodynamic distance to a phase boundary, and the proxy inherits the sampling density of the design; computing true boundary distances from a dense CALPHAD grid would decouple the two. Finally, the sparsemax and penalty conclusions are scoped to the tested hyperparameters, and the comparison set is not exhaustive over function classes: Gaussian-process/RBF interpolation, log-ratio (ALR/CLR/ILR) regression with zero replacement, Dirichlet-likelihood heads, and two-stage or presence-gated classify-then-regress architectures—the common remedy for the regressor–detector gap—were not evaluated. Three seeds quantify training stochasticity only, and per-experiment seed counts are small; the sparsemax variance claim in particular rests on three runs. All conclusions are furthermore scoped to three-input ternary systems; whether the MLP/tree crossover, the band-holdout behaviour, and the regressor–detector gap persist in higher-dimensional design spaces, where axis-aligned tree partitions lose their advantage, is untested, and a quaternary system with sample-size learning curves is the natural next experiment.

Another significant limitation of our current surrogate pipeline is its dependence on a predefined, closed phase set (K) determined prior to modeling. This static basis prevents the model from predicting or discovering previously unseen phases in unprobed compositional regions, and it also bounds what the strict extrapolation protocols can test: liquid lies outside the near-side basis in four of the five temperature-extrapolation systems, so part of the far-side error there is a basis limitation. Furthermore, our study did not apply log-ratio Compositional Data Analysis (CoDA) methods, such as the Centered Log-Ratio (CLR) or Isometric Log-Ratio (ILR) transformations, which are standard in geochemistry [15] and plant nutrition [16]. While CoDA elegantly handles simplex constraints, its mathematical formulations contain logarithmic terms that are undefined at zero. Managing the "structural zeros" (phases that are physically absent) which dominate multi-phase metallurgical equilibria remains an open challenge for CoDA, representing a promising direction for future scientific machine learning research.

# Conclusions

This study benchmarked six neural network output heads and four classical machine learning baselines across five Fe-based ternary systems, utilizing a mass-balance-validated dataset of 44,397 equilibria. The principal conclusions are as follows:

- Strict Constraint Adherence: Structurally constrained neural architectures—specifically softmax, sigmoid/Σ, and renorm heads—satisfy the full probability simplex constraint (mass-balance closure and strict non-negativity) natively at float32 precision without compromising regression accuracy. Unconstrained networks yield physically inadmissible outputs, violating closure by up to 8%.

- Topological Model Dependency: Model performance is strongly dependent on the phase diagram's topology: MLPs performed best in the two systems dominated by continuous, smooth phase coexistence fields, the random forest performed best in the one system defined by sharp, binary phase boundaries, and the remaining two systems were statistical ties (a 2–1–2 pattern across the five systems).

- The Regressor–Detector Gap: Regression accuracy does not guarantee reliable classification. The model yielding the lowest aggregate MAE may fail to detect trace phases, a vulnerability that becomes pronounced under the spatial holdouts evaluated here.

- Extrapolation Limits: While structurally constrained MLPs exhibited more robust in-hull spatial generalization compared to localized tree ensembles, true out-of-range extrapolation triggered severe, order-of-magnitude error degradation across all tested architectures; the temperature protocol is additionally limited by the closed phase basis, as liquid is unseen on the near-side training data in four of the five systems.

Practical Guidance: The sigmoid/Σ and softmax heads enforce closure natively at no measured accuracy cost and are sound defaults for phase-fraction regression; any workflow in which rare phases matter should complement the regressor with a dedicated presence detector or a presence-gated head (not evaluated here); band-limited spatial shifts are tolerable for constrained MLPs, whereas one-sided extrapolation should be treated as unsupported and re-validated with direct CALPHAD evaluation.

Code and Data Availability: The complete pipeline (TDB extraction, probe, data generation, training, evaluation, and all analyses reported in this paper, including the region-matched reanalysis, AUPRC, phase-rule admissibility, and the reconstruction of the design-space accounting) is available at [GitHub URL]. The five datasets (44,397 equilibria with per-phase fractions and thermodynamic potentials), the stored per-seed model predictions, and all result files are archived at [Zenodo DOI]. The MatCalc mc_fe_v2.062 source database is distributed under its own license and is not redistributed here; scripts reproducing the ternary extraction from a local copy are provided.

# References

1.	Yi Wang, W., et al., Integrated computational materials engineering for advanced materials: A brief review. Computational Materials Science, 2019. 158: p. 42-48.

2.	Bordonhos, M., et al., Multiscale Computational Approaches toward the Understanding of Materials. Advanced Theory and Simulations, 2023. 6(10): p. 2200628.

3.	Xi, S., et al., Phase diagram construction and prediction method based on machine learning algorithms. Journal of Materials Research and Technology, 2025. 36: p. 1917-1929.

4.	Liu, S., et al., A comparative study of predicting high entropy alloy phase fractions with traditional machine learning and deep neural networks. npj Computational Materials, 2024. 10(1): p. 172.

5.	Connolly, J.A.D., A primer in gibbs energy minimization for geophysicists. Petrology, 2017. 25(5): p. 526-534.

6.	Kim, S.W., et al., Estimating the phase volume fraction of multi-phase steel via unsupervised deep learning. Scientific Reports, 2021. 11(1): p. 5902.

7.	Xie, C., et al., From processing text to counterfactual steel design: a knowledge-graph-organized and reliability-aware machine learning framework. Materials & Design, 2026: p. 116691.

8.	Tahkola, M., et al., Accelerated discovery of Cr-based A2+B2 superalloys across 11 elements with a deep-learning CALPHAD surrogate. npj Computational Materials, 2026.

9.	Li, S., et al., Unsupervised Machine Learning Guides the Design of MnFeCoNiMg High-Entropy Alloys for Optimizing MoS2 Interface Properties. Journal of Materials Research and Technology, 2026.

10.	Vazquez, G., et al., A deep neural network regressor for phase constitution estimation in the high entropy alloy system Al-Co-Cr-Fe-Mn-Nb-Ni. npj Computational Materials, 2023. 9(1): p. 68.

11.	Yu, W., et al., Integrated design of hardness and weldability for multi-component Fe-based hardfacing alloys driven by machine learning and high-throughput computation. Journal of Materials Research and Technology, 2026. 42: p. 11496-11509.

12.	Mayr, L.M. and D. Bojanic, Novel trends in high-throughput screening. Current Opinion in Pharmacology, 2009. 9(5): p. 580-588.

13.	Zhang, T., et al., A self-adaptive deep learning algorithm for accelerating multi-component flash calculation. Computer Methods in Applied Mechanics and Engineering, 2020. 369: p. 113207.

14.	Ben Hicham, K.K., et al., Differentiable Thermodynamic Phase-Equilibria for Machine Learning. Journal of Chemical Information and Modeling, 2026.

15.	Meloni, F., et al., Integrating Compositional Data Analysis (CoDA) and Random Forest for lithology-specific geochemical baseline determination. Science of The Total Environment, 2026. 1011: p. 181169.

16.	Parent, L.E., Compositional and Machine Learning Tools to Model Plant Nutrition: Overview and Perspectives. Horticulturae, 2025. 11(2): p. 161.

17.	Karthik, M.R. and T.B. Rao, Physics-informed data-driven ensemble and transfer learning approaches for prediction of temperature field and cutting force during machining IN625 superalloy. International Journal on Interactive Design and Manufacturing (IJIDeM), 2025. 19(10): p. 7027-7060.

18.	Agrawal, A. and A. Choudhary, Perspective: Materials informatics and big data: Realization of the “fourth paradigm” of science in materials science. APL Materials, 2016. 4(5).

19.	Ward, L. and C. Wolverton, Atomistic calculations and materials informatics: A review. Current Opinion in Solid State and Materials Science, 2017. 21(3): p. 167-176.

20.	Li, K., et al., Probing out-of-distribution generalization in machine learning for materials. Communications Materials, 2025. 6(1): p. 9.

21.	Segal, N., et al., Known Unknowns: Out-of-Distribution Property Prediction in Materials and Molecules. npj Computational Materials, 2025. 11(1): p. 345.

22.	Li, X., et al., Combining transfer learning and statistical measures to predict performance of composite materials with limited data. Computer-Aided Civil and Infrastructure Engineering, 2025. 40(6): p. 817-838.

23.	Hatakeyama-Sato, K. and K. Oyaizu, Generative Models for Extrapolation Prediction in Materials Informatics. ACS Omega, 2021. 6(22): p. 14566-14574.

24.	Speckhard, D.T., et al., Extrapolation to the complete basis-set limit in density-functional theory using statistical learning. Physical Review Materials, 2025. 9(1): p. 013801.

25.	Li, Y., et al., Towards high-throughput microstructure simulation in compositionally complex alloys via machine learning. Calphad, 2021. 72: p. 102231.

26.	Rahnama, A., S. Clark, and S. Sridhar, Machine learning for predicting occurrence of interphase precipitation in HSLA steels. Computational Materials Science, 2018. 154: p. 169-177.

27.	Hao, S., et al., Developing reliable machine learning interatomic potential for Fe–Cr–Ni austenitic alloys. Journal of Applied Physics, 2025. 138(8).

28.	Panchal, J.H., S.R. Kalidindi, and D.L. McDowell, Key computational modeling issues in Integrated Computational Materials Engineering. Computer-Aided Design, 2013. 45(1): p. 4-25.

29.	Song, Y., et al., Prediction of clathrate hydrate phase equilibria using gradient boosted regression trees and deep neural networks. The Journal of Chemical Thermodynamics, 2019. 135: p. 86-96.

30.	Eiken, J., B. Böttger, and I. Steinbach, Multiphase-field approach for multicomponent alloys with extrapolation scheme for numerical application. Physical Review E—Statistical, Nonlinear, and Soft Matter Physics, 2006. 73(6): p. 066122.

31.	Anburaj, J., et al., Ageing of forged superaustenitic stainless steel: Precipitate phases and mechanical properties. Materials Science and Engineering: A, 2012. 535: p. 99-107.

32.	Aditya, D.M., et al., The study of sigma and carbide in cast austenitic stainless-steel grade HH after 24 years of high-temperature service. Heliyon, 2023. 9(3).