Simplex Constraints, Spatial Generalization, and the Regressor–Detector Gap in Machine-Learning Surrogates for CALPHAD Phase-Fraction Prediction

Sina Mousavia*, Narinderjit Singh Sawaran Singhb, Darya Ahmadovac, Sandeep Sharmad,e, Sanjeev Singhf,g, Qasem Kharmah

a Department of Computer Science Faculty of Statistics, Mathematics and Computer Science Allameh Tabataba'i University Tehran, Iran;

b Faculty of Data Science andInformation Technology, INTI International University, Persiaran Perdana BBN,Putra Nilai, Nilai, 71800, Negeri Sembilan, Malaysia;

c Azerbaijan State Oil and Industry University, Baku, Azerbaijan, AZ1010;

d Centre for Research Impact and Outcome, Chitkara University, Rajpura- 140417, Punjab, India;

e Center for innovation and inclusive research, Sharda University, Greater Noida, Uttar Pradesh, India;

f Noida Institute of Engineering and Technology, 19, Knowledge Park-II, Institutional Area, Greater Noida (UP)-201324, India.

g Division of research and development, lovely professional University, Phagwara, Punjab, India;

h Department of Software Engineering,Hourani Center for Applied Scientific Research, Al-Ahliyya Amman University, Amman, Jordan.

*Corresponding author, ss_mousavi@atu.ac.ir

Abstract:

Machine-learning surrogates massively accelerate CALPHAD equilibrium calculations, yet predicting multi-phase fractions introduces a strict physical requirement: outputs must reside on the probability simplex to conserve mass. Despite its necessity, a consensus on enforcing this constraint remains absent. To address this, we systematically benchmark six neural network output architectures against four classical baselines across 44,397 mass-balance-validated equilibria from five Fe-based ternary systems (Fe–Cr–Ni, Fe–Cr–Mn, Fe–Cr–Mo, Fe–Cr–V, Fe–Mn–Ni). We demonstrate that structurally constrained heads natively enforce mass balance to float32 precision without compromising continuous regression accuracy. Furthermore, predictive superiority is topologically dependent: constrained Multilayer Perceptrons (MLPs) excel in systems with smooth phase coexistence, whereas Random Forests dominate systems with sharp, binary boundaries. By utilizing size-matched random controls, we rigorously decouple data-volume penalties from spatial domain shifts across contiguous interior holdouts and strict one-sided extrapolation tasks. While MLPs degrade gracefully during in-hull shifts, true out-of-range extrapolation triggers catastrophic error degradation across all architectures. Additionally, we characterize a critical "regressor-detector gap," revealing that models minimizing aggregate regression error fail to detect rare trace phases, worsening severely under distribution shifts. Finally, detailing failed constraint mechanisms—including sparsemax, soft loss penalties, and residue closure—establishes robust guidelines for future materials informatics.

Keywords: CALPHAD; Machine learning surrogate; Simplex constraint; Spatial generalization; Phase fraction prediction.

# Introduction

The paradigm of Integrated Computational Materials Engineering (ICME) has fundamentally transformed modern alloy design by treating materials development as a concurrent, requirements-driven engineering process[1, 2]. At its core, ICME establishes tight, multiscale mathematical linkages across the processing–microstructure–property–performance chain, effectively replacing empirical trial-and-error with top-down computational design [2]. Within this framework, computational thermodynamics serves as the foundational connective tissue . The CALPHAD (CALculation of PHAse Diagrams) method provides high-fidelity database resources to predict stable equilibrium phase assemblages, transition temperatures, and thermodynamic properties as a rigorous function of temperature and local multi-component composition [3, 4].

These foundational calculations rely on the numerical minimization of a system's total Gibbs free energy under fixed temperature, pressure, and mass balance constraints [3, 5]. While alternative formulations have extended equilibrium calculations to other physical potentials [5], Gibbs energy minimization remains the standard. However, as metallurgical exploration shifts aggressively toward highly complex spaces—such as advanced high-strength steels [6, 7], multi-component superalloys [8], and high-entropy alloys [9]—computational alloy design is confronted by a massive combinatorial explosion of composition variables. Rigorous iterative equilibrium solvers are highly computationally intensive, often requiring several seconds to converge a single design coordinate [10]. When screening millions of potential chemistry combinations in high-dimensional composition spaces, the cumulative computational cost of raw CALPHAD queries becomes entirely prohibitive [9, 10].

To circumvent the bottlenecks inherent to iterative thermodynamic solvers, machine-learning (ML) surrogate models are increasingly deployed to replace raw CALPHAD queries [11]. These surrogates—ranging from tabular-oriented ensemble decision trees like Random Forests and XGBoost to deep neural networks (DNNs)—execute rapid forward passes that provide computational speedups of three to five orders of magnitude. Such massive acceleration enables the high-throughput screening of vast, multi-million composition databases in minutes rather than months [11, 12].

Despite these clear performance advantages, predicting multi-phase equilibria directly introduces a unique mathematical challenge: the predicted vector of equilibrium phase fractions must strictly reside on the probability simplex. To satisfy fundamental mass conservation laws, the phase fractions (Nk) for K possible phases must sum to exactly one and remain strictly non-negative [13]:

| k=1KNk=1, Nk≥0 | (1) |
| --- | --- |

Predictions that violate these structural constraints are physically inadmissible for downstream multiscale models, including kinetic simulations or phase-field modeling [14].

In adjacent fields like geochemistry [15] and agronomy [16], this challenge is addressed through Compositional Data Analysis (CoDA) using log-ratio transformations. In materials informatics, however, the literature exhibits a critical lack of consensus on how to best enforce these physical constraints on neural-network outputs [10]. Some researchers integrate standard softmax layers into multi-phase DNN regressors to natively restrict predictions to a sum of one [10, 13]. Others propose differentiable algorithms, such as DISCOMAX, which utilize straight-through softmax relaxations to guarantee thermodynamic consistency [14].

Conversely, recent deep-learning workflows focusing on complex superalloys found that enforcing a strict 100% sum rule on output heads actually reduced overall predictive accuracy. Consequently, those models defaulted to unconstrained linear outputs, deliberately accepting mass-balance errors to preserve continuous regression performance [17]. Alternative constraint configurations—such as post-hoc renormalization, sparsity-inducing operators like sparsemax, or algebraic residue closure—have been proposed, but their relative tradeoffs regarding predictive accuracy, physical admissibility, and training stability remain unbenchmarked in multi-phase metallurgical settings [14].

A secondary challenge in materials informatics is the evaluation of models beyond standard random or cluster-stratified cross-validation splits [18, 19]. Conventional protocols primarily assess interpolation ability, where queried test points are surrounded by local training neighbors [20]. Practical alloy discovery, however, frequently requires querying entirely unprobed chemical spaces. This introduces complex spatial generalization challenges: predictions must be made either in contiguous, missing interior regions or under strict out-of-range extrapolation [20, 21].

Evaluating surrogate models under these geometric distribution shifts is confounded by data volume. Removing a specific spatial region to construct a validation task inherently removes training data, making it statistically difficult to isolate the true algorithmic penalty of the spatial shift from the penalty of learning from a reduced dataset. Thus, establishing rigorous spatial generalization protocols utilizing size-matched random controls is mathematically necessary to decouple true spatial shifts from mere data-volume effects.

Furthermore, the architectural behavior of ML algorithms under these geometric shifts is starkly distinct. Tabular-oriented algorithms, such as Random Forests, interpolate systems dominated by sharp, binary phase boundaries well, but their step-function decision boundaries prevent them from predicting continuous trends beyond known ranges [4]. DNNs can produce smoother outputs that generalize more gracefully [4, 22]. Despite this potential, recent studies analyzing over 700 out-of-distribution (OOD) tasks demonstrate that true extrapolation beyond the training domain severely degrades predictive fidelity across all standard architectures [20]. To mitigate these limits, researchers have explored transductive approaches [21] or deep generative flow-based imputers [23]. However, a systematic, decoupled evaluation of spatial generalization limits for direct continuous phase fraction prediction remains absent.

An equally critical, yet often neglected, issue in evaluating CALPHAD surrogates is the regressor–detector gap. Standard validation almost exclusively relies on aggregate regression metrics, such as Mean Absolute Error (MAE) [24, 25]. Because zero-fraction rows mathematically dominate global loss calculations in multi-phase databases, an unconstrained model can achieve a deceptively low aggregate error by predicting near-zero fractions for inactive phases, while entirely failing to accurately resolve the emergence of newly stabilizing, rare phases.

In physical metallurgy, this specific modeling failure has severe real-world consequences. Detrimental intermetallic phases—such as the highly embrittling σ-phase in stainless steels—exercise a massively disproportionate influence on the alloy's mechanical toughness and corrosion properties despite small volume fractions [7, 26]. From a machine-learning perspective, standard uniform loss functions do not penalize their misprediction heavily enough to force gradient descent to learn their distinct, narrow thermodynamic boundaries. Consequently, a surrogate minimizing aggregate regression error is not necessarily an optimal phase-presence detector. This gap is robust across classification thresholds, and discrete phase-presence detection capability degrades much faster than continuous regression error under spatial distribution shifts. Resolving this gap is of paramount importance for building engineering trust in ML surrogates.

To address these interconnected challenges, this study systematically investigates how neural network architectures can reliably predict multi-phase equilibria while strictly satisfying physical mass conservation. Based on a highly comprehensive dataset of 44,397 rigorously validated thermodynamic equilibria generated via a transductive probing strategy of five Fe-based ternary systems (Fe–Cr–Ni, Fe–Cr–Mn, Fe–Cr–Mo, Fe–Cr–V, Fe–Mn–Ni), we evaluate the limits of deep learning surrogates under rigorous distribution shifts. These benchmark systems cover highly relevant metallurgical phases, including the industrially vital FCC solid-solution structures found in stainless steels and nickel-based superalloys.

The specific contributions of this work are fourfold: First, we benchmark six distinct neural network output configurations against four classical baselines to conclusively resolve how structural outputs affect both continuous regression accuracy and physical admissibility. Second, we establish decoupled spatial generalization protocols—a contiguous interior-band holdout and a strict one-sided extrapolation task—utilizing size-matched random controls to strictly decouple spatial penalties from data volume reductions. Third, we mathematically characterize the regressor–detector gap by analyzing a stable discrepancy between continuous regression error and discrete phase-presence detection under distribution shifts. Finally, we provide detailed reporting of informative negative results for three constraint mechanisms to establish clear design guidelines and prevent redundant algorithmic development in future ICME workflows.

# Methods

Figure 1 summarises the pipeline end to end: the CALPHAD data generation, the fixed-protocol split and model families, and the three evaluation protocols they are subjected to.

Figure 1. Study pipeline. (1) CALPHAD data generation: five Fe-based ternary subsystems are extracted from the open MatCalc steel database, probe-driven phase sets fix the target dimensionality, structured sampling draws 11,220 candidate points per system, and a mass-balance gate accepts 44,397 equilibria in total. (2) A cluster-stratified 64/16/20 split feeds a constrained MLP with six output heads (plus two mechanism probes) and four classical baselines, all fitted under one fixed protocol and three seeds. (3) Three evaluation protocols − interpolation, contiguous interior-band holdout, and strict one-sided extrapolation, the two spatial ones each with a size-matched random control — plus two secondary analyses (ablations and boundary-error analysis, dashed arrows).

## Data Generation

### Thermodynamic Description

All thermodynamic equilibrium calculations were driven by the open MatCalc steel database (mc_fe_v2.062). To ensure computational compatibility, a custom lenient parser was integrated with pycalphad to extract the relevant five ternary subsystems (Fe–Cr–Ni, Fe–Cr–Mn, Fe–Cr–Mo, Fe–Cr–V, and Fe–Mn–Ni) and implement minor syntax corrections. A rigorous validation step was performed on a pruned version of the database; this verified strict equivalence with the unpruned source, ensuring maximum deviations in phase fractions and Gibbs free energies remained strictly at zero across all systems. For all generated equilibria, the system pressure was fixed at 101,325 Pa.

### Probe-driven Phase Sets

Running complete equilibrium calculations with all eligible phases is computationally intensive, averaging roughly 2.5 seconds per query point. To streamline dataset generation, a transductive probing strategy was employed. Each of the five systems was independently sampled using 2,000 Dirichlet draws to identify which phases were actively present. As detailed in Table 1, only phases observed to be active during this probing phase were retained as regression targets, dramatically reducing the dimensionality (K) from the total eligible phases. This global preprocessing step definitively fixed the output dimensionality for each system prior to any predictive modeling. The fidelity of this phase-set reduction was strictly validated on an independent set of 1,500 points, confirming that the targets maintained mass-balance closure within the solver's tolerance bounds (|kyk-1|≤3.3×10-8).

Table 1. Summary of the investigated ternary systems, contrasting the total number of theoretically eligible phases against the verified probe-active target phases (K) utilized as regression targets in this study.

| System | x₂, x₃ | Eligible | K | Target phases |
| --- | --- | --- | --- | --- |
| Fe–Cr–Ni | Cr, Ni | 28 | 4 | BCC_A2, FCC_A1, LIQUID, SIGMA |
| Fe–Cr–Mn | Cr, Mn | 31 | 7 | ALPHA_MN, BCC_A2, BETA_MN, CR3MN5, FCC_A1, LIQUID, SIGMA |
| Fe–Cr–Mo | Cr, Mo | 29 | 9 | BCC_A2, CHI_A12, FCC_A1, LAVES_PHASE, LIQUID, MU_PHASE, MU_PHASE_I, R_PHASE, SIGMA |
| Fe–Cr–V | Cr, V | 25 | 4 | BCC_A2, FCC_A1, LIQUID, SIGMA |
| Fe–Mn–Ni | Mn, Ni | 29 | 7 | ALPHA_MN, BCC_A2, BETA_MN, FCC_A1, LIQUID, MNNI, MNNI2 |

### Sampling and Acceptance

The design variables for each system comprised two independent mole fractions (x2 and x3), with iron serving as the balance element (xFe=1-x2-x3), and temperature (T) sampled uniformly across the 700 to 2000 K domain. To prevent the systematic undersampling of metallurgically critical regions, five deterministic sampling strategies were combined to generate 11,220 candidate points per system. This approach deliberately over-represented the iron-rich corner, isothermal slices, the liquidus zone, and sigma-phase fields. A candidate data point was only incorporated into the final dataset if its composition resided within the defined sub-simplex and its computed equilibrium satisfied a stringent mass-balance tolerance (|kNk-1|<10-6). This acceptance protocol yielded robust datasets of approximately 8,880 convergent rows per ternary system, the statistical compositions of which are summarized in Table 2. The spatial distribution, phase occurrences, and structural closure bounds of this generated data are further visualized in Figure 2.

Table 2. Summary statistics of the generated datasets across the five Fe-based ternary systems, detailing phase occurrence boundaries and maximum deviations in mass-balance simplex closure.

| System | Rows | Box (%) | max¦Σy−1¦ | K | Occurrence range (%) |
| --- | --- | --- | --- | --- | --- |
| Fe–Cr–Ni | 8,880 | 38.0 | 9.8×10⁻⁹ | 4 | 11.94–73.6 |
| Fe–Cr–Mn | 8,880 | 38.0 | 1.2×10⁻⁸ | 7 | 0.03–57.5 |
| Fe–Cr–Mo | 8,877 | 38.0 | 3.3×10⁻⁸ | 9 | 0.10–63.5 |
| Fe–Cr–V | 8,880 | 38.0 | 1.9×10⁻⁸ | 4 | 2.04–79.9 |
| Fe–Mn–Ni | 8,880 | 38.0 | 1.9×10⁻⁹ | 7 | 0.00–76.0 |

Figure 2. Statistical overview of the generated datasets, with a detailed spatial visualization of the Fe–Cr–Ni system. (a) Design points in the composition plane colored by temperature. (b) Marginal density of sampled temperatures. (c) Demarcation of the industrially relevant stainless-steel subset. (d) Logarithmic frequency of target phase occurrences across all five systems. (e) Verification of mass-balance closure for target vectors prior to model training.

## Models and Training

### Neural-Network Architectures and Simplex Constraints

The core predictive model was a multilayer perceptron (MLP) featuring three hidden layers composed of 192 units each, integrated with LayerNorm, SiLU activations, and dropout regularization. Networks were trained via the AdamW optimizer employing cosine annealing, early stopping, and a Huber loss function (Δ=0.01). Features were standardized using scalers strictly fitted to the training partitions.

To rigorously assess the enforcement of the mass-balance constraint (Eq. 1), six distinct output heads were benchmarked:

- An unconstrained sigmoid baseline.

- A standard softmax projection.

- A train-time sigmoid/Σ normalization.

- A renorm head applying a sigmoid followed by clipping and post-hoc row-sum division.

- A sparsemax operator designed to produce exact zeros for absent phases.

- A residue closure head that algebraically infers the final phase fraction to enforce sum-to-one equality. Crucially, these models were evaluated not just for closure (summing to one) but for strict simplex membership (closure combined with strict non-negativity across all phase components).

### Baseline Models

To contextualize the neural network performance, four classical machine learning baselines were evaluated: ridge regression, distance-weighted k-nearest neighbors (k=10), XGBoost, and random forests. Because classical regressors do not intrinsically respect structural simplex constraints, each baseline was evaluated both in its raw predictive state and following post-hoc renormalization to yield physically admissible outputs.

### Splitting Protocols and Evaluation Metrics

For standard interpolation evaluations, data points were divided using a cluster-stratified KMeans split (k=6) to generate representative training (64%), validation (16%), and testing (20%) sets across the three-dimensional feature space. To account for stochastic training variance, all experiments were averaged over three distinct random initialization seeds. The primary continuous evaluation metric was the mean absolute error (MAE) computed across all phases. Phase-presence detection capabilities were additionally quantified using F1 scores and balanced accuracy, treating any phase with a predicted fractional presence exceeding 10-3 as physically active. All reported metrics are computed on the test partition, which played no role in training or early stopping. A phase with no active row in a given test set (MNNI2, with zero active rows in the whole Fe–Mn–Ni dataset) has an undefined F1; we score it as F1 = 0 for every model, which keeps the phase in the average without favoring any model. Table 6 additionally reports an entropy-weighted MAE, an auxiliary metric intended to up-weight multi-phase coexistence states, where several nonzero phase fractions must be predicted simultaneously; it is an evaluation aid, not a theoretically privileged loss.

## Spatial Generalization Evaluation Protocols

To explicitly test the spatial generalization and extrapolation limits of the surrogate models, two customized data splitting protocols were devised and executed in addition to the standard interpolation split:

- Contiguous Interior-Band Holdout: This protocol removed a specific temperature band (1200–1400 K) and a composition band (x2∈0.25,0.35) entirely from the training data. Delaunay triangulation confirmed that 99.3–99.4% of these held-out points remained within the convex hull of the surrounding training data, framing this as an in-hull distribution shift rather than strict extrapolation.

- Strict One-Sided Extrapolation: To test true out-of-range predictive capacity, models were trained exclusively on one side of a coordinate boundary (e.g., x2≤0.25) and tested strictly on the unobserved far side (e.g., x2>0.35).

A fundamental challenge in measuring spatial generalization is that removing a geometric region concurrently reduces the sheer volume of available training data. To deconvolve the spatial penalty from this data-volume penalty, both spatial protocols were evaluated alongside strictly sized-matched random controls. In these controls, an equivalent number of training rows were randomly excised across the entire domain, ensuring that any excess predictive degradation observed in the spatial holdouts was genuinely attributable to the domain shift rather than simple data scarcity.

# Results

## Predictive Accuracy on the Interpolation Split

The primary predictive performance of the evaluated surrogate models on the standard interpolation test sets is summarized in Table 3 and visualized in Figure 3. The comparative analysis reveals that no single architecture universally dominates across the five tested ternary systems. Instead, model superiority is strongly correlated with the underlying topological features of each phase diagram.

Constrained multilayer perceptrons (MLPs) demonstrated superior performance on systems characterized by extended, smooth multiphase coexistence fields. For the Fe–Cr–Ni system, the constrained renorm MLP achieved a mean absolute error (MAE) of 0.0106 ± 0.0006, significantly outperforming the random forest baseline (0.0180 ± 0.0002), representing a 41% reduction in error. A similar advantage was observed in the Fe–Cr–Mn system utilizing the sigmoid/Σ head. Conversely, tree-based models exhibited superior accuracy in systems dominated by sharp, essentially binary phase boundaries. In the Fe–Mn–Ni system, the random forest achieved an MAE of 0.0058 ± 0.0003, outperforming the best constrained MLP (0.0140 ± 0.0013). The Fe–Cr–Mo system resulted in a statistical tie between the two modeling paradigms, which was formally confirmed via paired bootstrap resampling over 10,000 iterations (Table 4).

Furthermore, the application of post-hoc renormalization to classical baseline models did not degrade predictive accuracy in any of the five evaluated systems; in fact, the projection reliably recovered valid states and marginally improved the error metrics.

Table 3. Interpolation test MAE across the five ternary systems, averaged over three random initialization seeds. Neural network heads are categorized by their structural adherence to the simplex constraint. Standard deviations are provided in the least significant digits.

| Group | Model | Fe–Cr–Ni | Fe–Cr–Mn | Fe–Cr–Mo | Fe–Cr–V | Fe–Mn–Ni |
| --- | --- | --- | --- | --- | --- | --- |
| off-simplex | sigmoid (unconstrained) | 0.0232 (10) | 0.0163 (1) | 0.0184 (5) | 0.0287 (4) | 0.0231 (13) |
| off-simplex | residue, y(d) = 1−Σ | 0.0229 (3) | 0.0186 (4) | 0.0182 (5) | 0.0254 (3) | 0.0210 (12) |
| on-simplex | sparsemax | 0.0444 (229) | 0.0212 (177) | 0.0573 (427) | 0.0304 (161) | 0.0375 (295) |
| on-simplex | softmax | 0.0130 (3) | 0.0088 (11) | 0.0148 (1) | 0.0167 (2) | 0.0145 (15) |
| on-simplex | sigmoid/Σ (train-time) | 0.0112 (10) | 0.0074 (2) | 0.0126 (2) | 0.0153 (4) | 0.0145 (20) |
| on-simplex | sigmoid + renorm (post hoc) | 0.0106 (6) | 0.0081 (4) | 0.0159 (3) | 0.0149 (4) | 0.0140 (13) |
| on-simplex | power-normalisation (†) | 0.0123 (14) | — | — | — | — |
| baselines | ridge | 0.2053 (9) | 0.1399 (5) | 0.1244 (6) | 0.1940 (8) | 0.0769 (5) |
| baselines | k-NN, k = 10 | 0.0256 (6) | 0.0171 (5) | 0.0151 (6) | 0.0222 (5) | 0.0091 (6) |
| baselines | XGBoost | 0.0212 (6) | 0.0154 (8) | 0.0137 (2) | 0.0179 (3) | 0.0081 (3) |
| baselines | random forest | 0.0180 (2) | 0.0133 (5) | 0.0123 (2) | 0.0137 (4) | 0.0058 (3) |

Table 4. Paired bootstrap statistical comparison of row-wise MAE differences between the best-performing constrained MLP and the random forest baseline on the interpolation test set (95% confidence interval, 10,000 resamples).

| System | Best MLP head | ΔMAE (MLP−RF) | 95% CI | Verdict |
| --- | --- | --- | --- | --- |
| Fe–Cr–Ni | renorm | -0.00737 | [-0.00850, -0.00627] | MLP better |
| Fe–Cr–Mn | sig-norm | -0.00593 | [-0.00670, -0.00514] | MLP better |
| Fe–Cr–Mo | sig-norm | +0.00027 | [-0.00054, +0.00109] | tie |
| Fe–Cr–V | renorm | +0.00115 | [-0.00071, +0.00303] | tie |
| Fe–Mn–Ni | renorm | +0.00821 | [+0.00678, +0.00970] | RF better |

Figure 3. Comparative regression accuracy and constraint adherence. (a) Mean test MAE for the evaluated neural network heads. (b) Relative MAE performance ratio of the best constrained MLP against the random forest baseline. (c) Quantification of simplex closure violations, demonstrating that structurally constrained heads and renormalized baselines satisfy mass-balance within machine precision bounds.

## Mass-Balance Simplex Closure

Enforcing the physical mass-balance requirement is critical for the admissibility of surrogate outputs in subsequent thermodynamic calculations. As detailed in Table 5, all structurally constrained neural network heads satisfied the closure equality constraint (kyk=1) to within 32-bit floating-point precision (≤5×10-8). In stark contrast, unconstrained sigmoid outputs violated this fundamental closure requirement by an average of 6% to 8%, and raw tree-based outputs exhibited violations between 0.9% and 4.7%. While post-hoc renormalization successfully repaired baseline outputs to machine precision (∼10-17), the structurally constrained MLPs achieved this physically admissible state natively without requiring secondary projection steps.

Table 5. Mean closure violations (|kyk-1|) on the test partition. Structurally constrained architectures achieve closure at float32 precision, while unconstrained models exhibit unphysical deviations spanning orders of magnitude.

| Closure | Model | Fe–Cr–Ni | Fe–Cr–Mn | Fe–Cr–Mo | Fe–Cr–V | Fe–Mn–Ni |
| --- | --- | --- | --- | --- | --- | --- |
| none | sigmoid | 6.2×10⁻² | 8.1×10⁻² | 8.1×10⁻² | 6.3×10⁻² | 7.4×10⁻² |
| none | random forest, raw | 2.8×10⁻² | 2.9×10⁻² | 4.7×10⁻² | 1.5×10⁻² | 8.7×10⁻³ |
| none | XGBoost, raw | 2.8×10⁻² | 3.3×10⁻² | 4.1×10⁻² | 2.1×10⁻² | 1.6×10⁻² |
| structural | softmax | 3.3×10⁻⁸ | 4.8×10⁻⁸ | 4.4×10⁻⁸ | 3.4×10⁻⁸ | 4.5×10⁻⁸ |
| structural | sigmoid/Σ | 1.7×10⁻⁸ | 2.7×10⁻⁸ | 3.3×10⁻⁸ | 1.6×10⁻⁸ | 3.1×10⁻⁸ |
| structural | sparsemax | 1.7×10⁻⁸ | 1.8×10⁻⁸ | 5.0×10⁻⁸ | 1.0×10⁻⁸ | 4.0×10⁻¹⁰ |
| structural | residue | 9.2×10⁻⁹ | 1.9×10⁻⁸ | 1.8×10⁻⁸ | 6.5×10⁻⁹ | 1.8×10⁻⁸ |
| post hoc | sigmoid + renorm | 1.5×10⁻⁸ | 2.5×10⁻⁸ | 2.5×10⁻⁸ | 1.2×10⁻⁸ | 3.3×10⁻⁸ |
| post hoc | random forest + renorm | 2.3×10⁻¹⁷ | 2.0×10⁻¹⁷ | 3.8×10⁻¹⁷ | 1.5×10⁻¹⁷ | 8.9×10⁻¹⁸ |

## The Regressor–Detector Gap

A critical distinction emerged between continuous regression accuracy (MAE) and discrete phase-presence detection (quantified via F₁ scores and balanced accuracy). As summarized in Table 6 and Figure 4, the model minimizing aggregate MAE is not necessarily the optimal phase-presence detector. This discrepancy is largely attributed to the sparsity of rare phases: zero-fraction rows dominate the global loss calculation, meaning a model can achieve a low aggregate MAE while entirely failing to resolve a trace phase. For example, in the Fe–Mn–Ni system, the MLP failed to detect three rare phases (F₁ = 0), whereas the random forest successfully resolved two of them.

This regressor–detector gap proved robust across varying classification thresholds. Sensitivity analyses evaluating phase presence thresholds of 10⁻⁴, 10⁻³, and 10⁻² (Table 7) confirmed that while absolute F₁ scores shifted as expected, the relative rank order of model detection capability remained highly stable across four of the five systems. Crucially, phase-presence detection was observed to be highly sensitive to distribution shifts; on the held-out temperature band of the Fe–Cr–Ni system, the MLP's mean F₁ score degraded from 0.93 to 0.64, even as continuous MAE remained relatively stable.

Table 6. Quantitative comparison of continuous regression performance (MAE) versus discrete phase-presence detection (F₁ score and balanced accuracy). The data highlight that optimal regression performance does not inherently guarantee optimal phase detection.

| System | Model | MAE | F₁ | Bal. acc. | Entropy-w. MAE |
| --- | --- | --- | --- | --- | --- |
| Fe–Cr–Ni | MLP renorm | 0.0106 | 0.927 | 0.939 | 0.0137 |
|  | random forest | 0.0180 | 0.846 | 0.887 | 0.0218 |
| Fe–Cr–Mn | MLP sig-norm | 0.0074 | 0.527 | 0.752 | 0.0089 |
|  | random forest | 0.0133 | 0.592 | 0.850 | 0.0150 |
| Fe–Cr–Mo | MLP sig-norm | 0.0126 | 0.643 | 0.827 | 0.0149 |
|  | random forest | 0.0123 | 0.629 | 0.858 | 0.0147 |
| Fe–Cr–V | MLP renorm | 0.0149 | 0.718 | 0.822 | 0.0167 |
|  | random forest | 0.0137 | 0.785 | 0.893 | 0.0158 |
| Fe–Mn–Ni | MLP renorm | 0.0140 | 0.312 | 0.643 | 0.0158 |
|  | random forest | 0.0058 | 0.504 | 0.884 | 0.0063 |

Table 7. Sensitivity analysis of phase-presence detection metrics as a function of the minimum fractional presence threshold, confirming the stability of the observed regressor–detector gap.

| System | Model | F₁ at 10⁻⁴ | F₁ at 10⁻³ | F₁ at 10⁻² |
| --- | --- | --- | --- | --- |
| Fe–Cr–Ni | best MLP (renorm) | 0.870 (6) | 0.927 (4) | 0.962 (3) |
|  | random forest | 0.815 (6) | 0.846 (6) | 0.911 (2) |
| Fe–Cr–Mn | best MLP (sig-norm) | 0.489 (6) | 0.527 (2) | 0.550 (2) |
|  | random forest | 0.571 (20) | 0.592 (18) | 0.672 (19) |
| Fe–Cr–Mo | best MLP (sig-norm) | 0.562 (13) | 0.643 (2) | 0.710 (3) |
|  | random forest | 0.590 (2) | 0.629 (3) | 0.727 (4) |
| Fe–Cr–V | best MLP (renorm) | 0.671 (35) | 0.718 (1) | 0.731 (1) |
|  | random forest | 0.767 (6) | 0.785 (9) | 0.870 (6) |
| Fe–Mn–Ni | best MLP (renorm) | 0.306 (5) | 0.312 (4) | 0.314 (4) |
|  | random forest | 0.470 (0) | 0.504 (1) | 0.603 (21) |

Figure 4. Analysis of the regressor–detector gap. (a) Parity plot contrasting the predictive accuracy of the most frequent versus least frequent phases in the Fe–Cr–Ni system. (b) Correlation between per-phase MAE and overall phase occurrence frequency. (c) Ratio comparison of MAE against F₁ score, illustrating domains where optimal regressors act as inferior detectors.

## Spatial Generalization and Extrapolation Limits

The models were subjected to rigorous spatial generalization tests utilizing strictly sized-matched random controls to decouple spatial degradation from training data attrition.

Contiguous Interior-Band Holdout: Results for the missing-region generalization test (Table 8, Figure 5a) demonstrated that degradation on the held-out temperature band was largely attributable to the reduced data volume; both the MLP and the random forest paid an equivalent 1.31× penalty ratio relative to their matched controls on the Fe–Cr–Ni system. However, performance separated significantly on the composition holdout band, which spanned steep phase boundaries. Across systems containing contiguous compositional holdouts, constrained MLPs degraded more gracefully than tree-based models, yielding a consistently lower penalty ratio (e.g., 1.61× versus 3.11× for the random forest on Fe–Cr–Ni).

Strict One-Sided Extrapolation: As detailed in Table 9 and Figure 6, true out-of-range extrapolation yielded severe degradation across all evaluated model families. For compositional extrapolation in the Fe–Cr–Ni system, MAE deteriorated by an order of magnitude, rising to ~0.17 for the constrained MLP and ~0.22 for the random forest, relative to ~0.012 on the matched interpolation controls. While the constrained MLP consistently achieved the lowest absolute far-side error across all five systems in both composition and temperature extrapolation, the overarching result underscores that no current architecture extrapolated phase fractions reliably beyond the explicit limits of the training domain.

Table 8. Predictive degradation under contiguous interior-band holdouts. Penalty ratios strictly compare the holdout error against a size-matched random control, isolating the spatial penalty from data-volume effects.

| Held-out region | Model | Fe–Cr–Ni | Fe–Cr–Mn | Fe–Cr–Mo | Fe–Cr–V | Fe–Mn–Ni |
| --- | --- | --- | --- | --- | --- | --- |
| random control | MLP renorm | 0.0101 (8) | 0.0083 (6) | 0.0153 (5) | 0.0234 (70) | 0.0122 (2) |
| random control | MLP sigmoid/Σ | 0.0107 (10) | 0.0077 (6) | 0.0125 (7) | 0.0146 (13) | 0.0123 (1) |
| random control | random forest | 0.0198 (11) | 0.0142 (5) | 0.0140 (11) | 0.0155 (12) | 0.0058 (4) |
| random control | XGBoost | 0.0237 (9) | 0.0167 (6) | 0.0152 (11) | 0.0194 (7) | 0.0084 (1) |
| T ∈ [1200, 1400] K | MLP renorm | 0.0132 (9) | 0.0079 (4) | 0.0266 (4) | 0.0358 (3) | 0.0022 (0) |
| T ∈ [1200, 1400] K | MLP sigmoid/Σ | 0.0144 (32) | 0.0077 (0) | 0.0265 (4) | 0.0372 (12) | 0.0024 (2) |
| T ∈ [1200, 1400] K | random forest | 0.0258 (10) | 0.0123 (2) | 0.0309 (12) | 0.0762 (97) | 0.0090 (6) |
| T ∈ [1200, 1400] K | XGBoost | 0.0408 (17) | 0.0203 (16) | 0.0348 (17) | 0.0823 (77) | 0.0167 (7) |
| x₂ ∈ [0.25, 0.35] | MLP renorm | 0.0162 (7) | 0.0071 (0) | 0.0155 (5) | 0.0111 (52) | 0.0005 (0) |
| x₂ ∈ [0.25, 0.35] | MLP sigmoid/Σ | 0.0163 (6) | 0.0071 (3) | 0.0144 (7) | 0.0075 (15) | 0.0010 (5) |
| x₂ ∈ [0.25, 0.35] | random forest | 0.0615 (73) | 0.0223 (6) | 0.0259 (9) | 0.0288 (5) | 0.0043 (1) |
| x₂ ∈ [0.25, 0.35] | XGBoost | 0.0530 (22) | 0.0250 (11) | 0.0324 (3) | 0.0368 (27) | 0.0063 (7) |
| penalty T / x₂ | MLP renorm | 1.31 / 1.61 | 0.95 / 0.85 | 1.74 / 1.01 | 1.53 / 0.48 | 0.18 / 0.04 |
| penalty T / x₂ | MLP sigmoid/Σ | 1.34 / 1.52 | 1.00 / 0.92 | 2.12 / 1.16 | 2.55 / 0.52 | 0.20 / 0.08 |
| penalty T / x₂ | random forest | 1.31 / 3.11 | 0.86 / 1.57 | 2.21 / 1.85 | 4.92 / 1.86 | 1.54 / 0.73 |
| penalty T / x₂ | XGBoost | 1.72 / 2.24 | 1.21 / 1.49 | 2.29 / 2.13 | 4.24 / 1.89 | 2.00 / 0.75 |

Table 9. Absolute MAE and penalty ratios for strict one-sided extrapolation beyond the established bounds of the training coordinates. All models exhibit sharp error increases under genuine extrapolation.

| Region | Model | Fe–Cr–Ni | Fe–Cr–Mn | Fe–Cr–Mo | Fe–Cr–V | Fe–Mn–Ni |
| --- | --- | --- | --- | --- | --- | --- |
| random control (x₂-matched) | MLP renorm | 0.0123 (3) | 0.0094 (2) | 0.0181 (5) | 0.0242 (73) | 0.0135 (6) |
| random control (x₂-matched) | MLP sigmoid/Σ | 0.0128 (16) | 0.0092 (3) | 0.0144 (5) | 0.0163 (13) | 0.0146 (10) |
| random control (x₂-matched) | random forest | 0.0236 (7) | 0.0168 (1) | 0.0167 (6) | 0.0191 (11) | 0.0084 (2) |
| random control (x₂-matched) | XGBoost | 0.0283 (14) | 0.0202 (7) | 0.0184 (5) | 0.0235 (16) | 0.0118 (2) |
| train x₂ ≤ 0.25, test x₂ > 0.35 | MLP renorm | 0.1721 (77) | 0.0458 (17) | 0.0668 (26) | 0.0464 (66) | 0.0143 (25) |
| train x₂ ≤ 0.25, test x₂ > 0.35 | MLP sigmoid/Σ | 0.1709 (65) | 0.0526 (28) | 0.0689 (8) | 0.0478 (60) | 0.0129 (8) |
| train x₂ ≤ 0.25, test x₂ > 0.35 | random forest | 0.2152 (9) | 0.0788 (5) | 0.1052 (22) | 0.0761 (50) | 0.0279 (6) |
| train x₂ ≤ 0.25, test x₂ > 0.35 | XGBoost | 0.2267 (28) | 0.0860 (47) | 0.1082 (12) | 0.1015 (38) | 0.0329 (3) |
| random control (T-matched) | MLP renorm | 0.0127 (2) | 0.0100 (2) | 0.0187 (8) | 0.0277 (4) | 0.0142 (5) |
| random control (T-matched) | MLP sigmoid/Σ | 0.0142 (12) | 0.0102 (3) | 0.0153 (4) | 0.0158 (8) | 0.0151 (4) |
| random control (T-matched) | random forest | 0.0245 (10) | 0.0178 (5) | 0.0173 (6) | 0.0194 (17) | 0.0080 (3) |
| random control (T-matched) | XGBoost | 0.0285 (14) | 0.0214 (3) | 0.0191 (5) | 0.0243 (18) | 0.0111 (1) |
| train T ≤ 1200 K, test T > 1400 K | MLP renorm | 0.2227 (66) | 0.1262 (41) | 0.0823 (27) | 0.0994 (6) | 0.1823 (0) |
| train T ≤ 1200 K, test T > 1400 K | MLP sigmoid/Σ | 0.2241 (96) | 0.1266 (48) | 0.0796 (19) | 0.0991 (11) | 0.1822 (0) |
| train T ≤ 1200 K, test T > 1400 K | random forest | 0.2346 (4) | 0.1524 (13) | 0.1073 (8) | 0.1937 (10) | 0.1834 (1) |
| train T ≤ 1200 K, test T > 1400 K | XGBoost | 0.2327 (6) | 0.1536 (16) | 0.1054 (5) | 0.1972 (20) | 0.1841 (2) |
| penalty x₂ / T | MLP renorm | 13.98 / 17.60 | 4.89 / 12.57 | 3.69 / 4.40 | 1.92 / 3.59 | 1.06 / 12.85 |
| penalty x₂ / T | MLP sigmoid/Σ | 13.36 / 15.78 | 5.74 / 12.46 | 4.78 / 5.19 | 2.93 / 6.25 | 0.88 / 12.05 |
| penalty x₂ / T | random forest | 9.12 / 9.56 | 4.69 / 8.55 | 6.29 / 6.21 | 3.99 / 9.97 | 3.30 / 22.84 |
| penalty x₂ / T | XGBoost | 8.02 / 8.16 | 4.25 / 7.19 | 5.87 / 5.51 | 4.31 / 8.11 | 2.79 / 16.64 |

Figure 5. Generalization degradation analyses. (a) Penalty ratios corresponding to the contiguous interior-band holdouts. (b) Effect of neural network hidden-layer width on predictive accuracy. (c) Sensitivity of the renorm and sigmoid/Σ heads to the selection of the loss function.

Figure 6. Strict one-sided extrapolation evaluation. (a) Penalty ratios for compositional and temperature extrapolation versus size-matched controls. (b) Absolute test MAE values on the extrapolated far side, highlighting the persistent challenge of out-of-support prediction.

## Model Ablations

To dissect the architectural dependencies of the neural network surrogates, a series of ablation studies were performed on the Fe–Cr–Ni system (Table 10, Figures 5b and 5c). The selection of loss function proved highly influential; mean squared error (MSE) exacerbated MAE by 47% relative to Huber (Δ=0.01) or standard MAE losses, primarily because trace phase outliers disproportionately skewed the squared gradient. Increasing hidden-layer capacity from 64 to 256 units monotonically improved accuracy, indicating that the default 192-unit architecture used across the benchmarking suite leaves further optimization headroom. Crucially, attempting to enforce mass balance via a soft sum-to-one loss penalty (λ=1 and λ=10) degraded the overall fit by a factor of 8 to 16 without achieving the numerical strictness provided by structural output constraints.

Table 10. Architectural ablation study for the Fe–Cr–Ni system, evaluating the impacts of loss function formulation, network capacity, and soft closure penalties on the interpolation MAE.

| Ablation | Setting | renorm | sigmoid/Σ |
| --- | --- | --- | --- |
| loss | Huber, δ = 0.01 (default) | 0.0106 (6) | 0.0112 (10) |
| loss | MAE | 0.0103 (6) | 0.0112 (4) |
| loss | MSE | 0.0156 (5) | 0.0152 (6) |
| width | 3×64 | 0.0137 (6) | 0.0139 (10) |
| width | 3×128 | 0.0114 (5) | 0.0131 (17) |
| width | 3×192 (default) | 0.0106 (6) | 0.0112 (10) |
| width | 3×256 | 0.0099 (7) | 0.0105 (7) |
| closure penalty | none | 0.0232 (10), closure 6.2×10⁻² |  |
| closure penalty | λ=1 | 0.0804 (51), closure 2.2×10⁻³ |  |
| closure penalty | λ=10 | 0.1693 (228), closure 1.3×10⁻³ |  |

## Evaluation of Failed Constraint Mechanisms (Negative Results)

Three theoretically plausible physical constraint mechanisms failed under the evaluated configurations (Figure 7), providing critical mechanistic insights into model formulation:

- Sparsemax: While successfully projecting logits to produce exact zeros, this operator exhibited severe seed sensitivity. The resulting inter-seed variance was on the same order of magnitude as the mean MAE, consistent with the hypothesis that gradients vanish identically once a logit drops below the threshold, trapping the network in poor initial local minima.

- Sum-to-One Penalty: As noted in the ablations, enforcing mass balance strictly as a regularizing loss term created pathological competition with the regression targets, buying partial closure entirely at the expense of model fit.

- Residue Closure: The algebraic deduction of the K-th phase fraction (yK=1-k<Kyk) enforces sum-to-one closure by construction but does not intrinsically guarantee non-negativity: if the other predicted fractions sum to more than one, the residue is negative. In the stored predictions, the residue head emitted negative values on 0.0% (Fe–Cr–V), 0.02% (Fe–Mn–Ni), 0.40% (Fe–Cr–Ni), 0.50% (Fe–Cr–Mn), and 1.21% (Fe–Cr–Mo) of cells, with the most negative cell at −0.59. It is therefore closure-valid but not simplex-valid. It was also the least accurate constrained variant: even the best residue head was 1.3–2.5× worse than the best constrained head in the same system, and a sweep over all K choices of the dropped phase (Figure 7c) shows the best choice is the dominant phase in four of five systems. The observed degradation is consistent with the residual phase absorbing the accumulated prediction error of the other K−1 channels; we note this as an interpretation supported by the sweep, not a directly demonstrated mechanism.

Figure 7. Diagnostic overview of failed constraint mechanisms. (a) Severe seed sensitivity and variance observed using the sparsemax operator. (b) The detrimental tradeoff between enforcing a soft closure penalty and maintaining regression accuracy. (c) Error accumulation in the residue closure head as a function of the chosen residual phase.

## Phase Field Visualization and Error Concentration

Qualitative and quantitative assessments of the predicted phase fields (Figure 8) underscore the topological nature of the surrogate errors. Visual analysis of the Fe–Cr–Ni domain under the renorm head confirms that the neural surrogate faithfully reproduces the complex geometry of the underlying CALPHAD phase fields, accurately mapping the BCC, FCC, liquid, and sigma topologies.

However, mapping the spatial distribution of the absolute error reveals significant spatial concentration. By computing the parametric distance of each test row to the nearest shift in the active-phase set, it was determined that mean absolute errors in the closest spatial tertile to a phase boundary averaged 0.022, compared to 0.002 in the most distant interior tertile. This indicates that surrogate uncertainty is highly concentrated directly at structural phase boundaries, whereas the interior of single- or stable multi-phase fields is reproduced with an order of magnitude higher fidelity.

Figure 8. Ground-truth and predicted phase-fraction fields for the Fe–Cr–Ni system evaluated with the renorm head. The absolute error maps highlight the geometric concentration of predictive uncertainty at phase boundaries relative to the stable interiors of phase fields.

# Discussion

## Topological Dependencies and Spatial Concentration of Error

The primary finding from our standard interpolation benchmarking (Table 3, Figure 3) is that the optimal machine learning architecture is not a universal construct; rather, it is fundamentally dictated by the physical-topological characteristics of the underlying thermodynamic phase diagram [10].

In alloy systems dominated by wide, continuously transitioning multi-phase fields, Deep Neural Networks (DNNs) with smooth, structurally constrained output heads (such as standard softmax or train-time sigmoid/Σ normalization) demonstrate clear superiority [4]. This behavior is prominent in the Fe–Cr–Ni, Fe–Cr–Mn, and Fe–Cr–Mo systems. For example, the Fe–Cr–Ni system features a wide face-centered cubic (FCC) solid-solution matrix transitioning smoothly into body-centered cubic (BCC) and topologically close-packed (TCP) σ intermetallics [27, 28]. The continuous, highly differentiable parameterization of Multilayer Perceptrons (MLPs) naturally aligns with these smooth thermodynamic fraction gradients, allowing the network to regress phase fraction shifts with high fidelity.

Conversely, in alloy systems governed by steep, nearly vertical phase boundaries—such as the sharp FCC-to-liquid boundaries in Fe–Mn–Ni or the abrupt BCC-to-σ transitions in Fe–Cr–V—classical tree-based architectures (such as Random Forests and XGBoost) achieve superior interpolation performance [4, 29]. The axis-aligned partitioning logic of decision trees is highly efficient at representing step-like, non-differentiable phase boundaries without artificially smoothing the transitions. However, this topological model dependency reveals a severe limitation: tree-based models lack the smooth extrapolation and continuous interpolation capabilities necessary for multi-scale simulations, such as phase-field modeling [30].

Furthermore, irrespective of the chosen model family, predictive uncertainty is geometrically constrained by the phase diagram topology. By mapping the spatial distribution of the absolute error of our surrogate models (Figure 8), we observe that predictive error is not uniformly distributed across the composition–temperature space. Instead, absolute errors are profoundly concentrated at the phase boundaries—where the active-phase set changes. Under the best-performing constrained MLP (the renorm head in Fe–Cr–Ni), the mean absolute error (MAE) in the spatial tertile closest to a phase boundary averages 0.022, whereas the stable interiors of single-phase or multi-phase fields are reproduced with near-perfect precision, averaging 0.002 (an order of magnitude lower). This spatial concentration of error highlights that surrogate model evaluations should move beyond simple global metrics (such as aggregate MAE) to incorporate spatially resolved topological diagnostics (see Figure 8).

## The Reality of Spatial Generalization in Alloy Design

Evaluating machine learning surrogates beyond standard random cross-validation splits is essential for assessing their viability in actual alloy discovery workflows. Random splitting assumes that the test set is independent and identically distributed (i.e., interpolation), but practical alloy design frequently requires navigating "holes" in experimental or computational data, or exploring entirely unprobed chemical spaces [20]. Our spatial generalization protocols explicitly test these out-of-distribution (OOD) boundaries by separating spatial shift penalties from simple data-volume constraints.

Under contiguous, in-hull spatial shifts—simulating missing interior data such as a temperature-band holdout (T∈1200,1400 K) or a composition-band holdout (x2∈0.25,0.35)—MLPs degrade much more gracefully than tree-based models. As visualized in Figure 5, the penalty ratio (the ratio of OOD error to a size-matched random control error) remains between 1.0 and 2.5 for the constrained MLPs, whereas it spikes up to 3.1 to 4.9 for Random Forests and XGBoost. Tree-based models rely on localized leaf-value averages and collapse abruptly near the boundaries of missing bands, returning step-like predictions that are highly unphysical. In contrast, the continuous mathematical representations of MLPs bridge these spatial gaps smoothly, making them far more robust for "filling in" missing thermodynamic coordinate spaces.

However, this graceful in-hull degradation must not be conflated with true thermodynamic extrapolation. When subjected to strict, out-of-range, one-sided extrapolation (e.g., training on x2≤0.25 and testing on x2>0.35, or training on T≤1200 K and testing on T>1400 K), predictive accuracy collapses catastrophically across all architectures. Absolute MAEs on the far-side climb to 0.17 to 0.22, representing a 10-to-20-fold degradation compared to matched interpolation controls (Figure 6). This severe degradation aligns with extensive out-of-distribution materials informatics benchmarks of over 700 OOD tasks, which show that standard deep learning architectures struggle with true extrapolation because the target spaces fall outside their representational support. Merely scaling up dataset size or training time yields diminishing returns in these extrapolative regimes, necessitating alternative transductive architectures that learn relative property changes rather than absolute values, or deep generative flow-based models to "imagine" missing boundaries [23].

## Thermodynamic Fidelity versus Numerical Emulation

To establish a rigorous epistemic foundation for materials informatics, we must distinguish between thermodynamic physical truth and numerical emulation. A machine learning surrogate is not a physical theory; it is strictly a high-speed numerical emulator trained to approximate the outputs of an underlying CALPHAD solver, executing the mapping:

x,T→yCALPHAD

Consequently, the surrogate model intrinsically inherits all underlying thermodynamic assumptions (such as global equilibrium postulates) and databases (such as MatCalc mc_fe_v2.062) used to generate the training data. High accuracy on a test partition simply confirms that the neural network has successfully emulated the solver's numerical optimization to float32 precision. It does not validate the physical accuracy of the CALPHAD model itself. For example, if a CALPHAD database fails to capture a metastable phase due to a lack of assessed binary or ternary interaction parameters [8], the surrogate will mathematically replicate this blind spot.

This distinction emphasizes the role of surrogates as high-speed screening filters rather than thermodynamic arbiters. While the 104-fold speedups provided by MLPs enable the screening of multi-million composition databases in seconds, any candidate alloy identified during high-throughput screening must be independently re-validated using direct CALPHAD calculations and, ultimately, targeted experimental synthesis.

## The Metallurgy of the Regressor–Detector Gap

A critical, often neglected issue in materials informatics is the "regressor–detector gap," where models optimized for continuous regression (lowest overall MAE) act as poor phase-presence detectors [24]. In physical metallurgy, minor or rare phases exercise a disproportionate influence on an alloy's properties. For example, the presence of trace intermetallics (such as the embrittling σ-phase in stainless steels) or minor reinforcing carbides can completely alter mechanical strength, creep resistance, and corrosion properties [31, 32].

From a machine-learning perspective, these rare phases are cheap in terms of global loss calculations. Because zero-fraction rows mathematically dominate the multi-phase alloy database (as candidate phases are absent across vast composition–temperature coordinates), a model can achieve a deceptively low aggregate MAE of 0.007 by predicting near-zero fractions for inactive phases, while entirely failing to resolve the stabilizing boundaries of rare, trace, or minor phases.

As detailed in Table 6, this leads to a stable discrepancy: in the Fe–Cr–Mn system, the MLP achieves the lowest continuous regression error yet the random forest is the better detector; in the Fe–Mn–Ni system, the random forest wins both tasks, while the MLP exhibits an exceptionally poor F1 score (0.312) and fails to detect three rare phases entirely (MNNI, MNNI2, and ALPHA_MN). In contrast, the random forest pairs the lowest continuous error in that system with a significantly more robust detector (F1 score of 0.504). This regressor–detector gap is robust across varying classification thresholds (10-4 to 10-2), and more importantly, discrete phase-presence detection capability degrades much faster than continuous regression error when the model is subjected to spatial distribution shifts. This finding suggests that future materials informatics workflows must utilize multi-criteria validation, incorporating classification-based metrics (such as F1 scores and balanced accuracy) alongside continuous regression errors to build reliable surrogates.

## Limitations and Mechanistic Insights from Negative Results

A primary value of this study lies in the detailed characterization of negative results, which establishes clear mathematical boundaries and prevents redundant developmental efforts in materials informatics. Three theoretically plausible constraint mechanisms failed to perform reliably:

- Sparsemax Operator (Figure 7a): While sparsemax mathematically projects logits onto the simplex to output exact zeros, it exhibited severe seed sensitivity. The resulting inter-seed variance was on the same order of magnitude as the mean MAE. This behavior is consistent with the hypothesis that gradients vanish identically once a logit drops below the threshold, trapping the network in poor initial local minima and making training highly unstable.

- Sum-to-One Soft Optimization Penalty (Figure 7b): Attempting to enforce mass-balance closure strictly as a regularizing loss term (e.g., λ=1 or λ=10) created pathological competition with the regression targets. It purchased partial closure entirely at the expense of model fit, degrading the overall MAE by a factor of 8 to 16. For the tested formulation and penalty weights, the soft penalty was redundant and strongly detrimental; structural output layers achieved numerical closure without sacrificing the fit.

- Residue Closure Head (Figure 7c): Algebraically deducing the K-th phase fraction as a residual (NK=1-k<KNk) accumulated all individual neural prediction errors into a single, unconstrained channel. This led to massive error accumulation in the designated residual phase and frequently produced physically inadmissible negative fractions; under the evaluated configuration, this asymmetrical closure formulation proved unviable.

Several protocol-level caveats bound the generality of these findings. The contiguous-band holdout is a missing-region test inside the sampled domain, and the strict extrapolation protocol is one-sided, covering only one coordinate at a time; behavior beyond the sampled simplex remains unvalidated. The design distribution is deliberately structured, not uniform, so all reported average errors are expectations under that sampling distribution, and rankings could shift under a different prior. All MLPs share one fixed architecture and all baselines use fixed hyperparameters: the comparison is a fixed-protocol benchmark, not an exhaustive hyperparameter search, and the reported MLP is not architecture-optimal. The mean ± standard deviation over three seeds quantifies seed-to-seed training stochasticity only, not total predictive uncertainty. The phase-boundary analysis uses an empirical boundary proxy — the distance to the nearest sampled row with a different active-phase set — not the exact thermodynamic distance to a phase boundary. Finally, the sparsemax and penalty conclusions are scoped to the tested hyperparameters, and the comparison set is not exhaustive over function classes.

Another significant limitation of our current surrogate pipeline is its dependence on a predefined, closed phase set (K) determined prior to modeling. This static basis prevents the model from predicting or discovering previously unseen phases in unprobed compositional regions. Furthermore, our study did not apply log-ratio Compositional Data Analysis (CoDA) methods, such as the Centered Log-Ratio (CLR) or Isometric Log-Ratio (ILR) transformations, which are standard in geochemistry [15] and plant nutrition [16]. While CoDA elegantly handles simplex constraints, its mathematical formulations contain logarithmic terms that are undefined at zero. Managing the "structural zeros" (phases that are physically absent) which dominate multi-phase metallurgical equilibria remains a massive challenge for CoDA, representing an exciting and vital direction for future scientific machine learning research.

# Conclusions

This study benchmarked six neural network output heads and four classical machine learning baselines across five Fe-based ternary systems, utilizing a mass-balance-validated dataset of 44,397 equilibria. The principal conclusions are as follows:

- Strict Constraint Adherence: Structurally constrained neural architectures—specifically softmax, sigmoid/Σ, and renorm heads—satisfy the full probability simplex constraint (mass-balance closure and strict non-negativity) natively at float32 precision without compromising regression accuracy. Unconstrained networks yield physically inadmissible outputs, violating closure by up to 8%.

- Topological Model Dependency: Model superiority is highly dependent on the phase diagram's topology. MLPs excel in systems dominated by continuous, smooth phase coexistence fields, whereas random forests outperform in systems defined by sharp, binary phase boundaries.

- The Regressor–Detector Gap: Regression accuracy does not guarantee reliable classification. The model yielding the lowest aggregate MAE may fail to detect trace phases, a vulnerability that becomes sharply pronounced under spatial distribution shifts.

- Extrapolation Limits: While structurally constrained MLPs exhibited more robust in-hull spatial generalization compared to localized tree ensembles, true out-of-range extrapolation triggered severe, order-of-magnitude error degradation across all tested architectures.

# Code and Data Availability

The code and data supporting the findings of this study are publicly available on GitHub: https://github.com/user4072/CALPHAD-based-Phase-Fraction-Prediction

# CRediT Author Statement

- Sina Mousavi: Conceptualization, Methodology, Software, Data curation, Formal analysis, Investigation, Visualization, Writing – original draft, Project administration.

- Narinderjit Singh Sawaran Singh: Methodology, Formal analysis, Validation, Writing – review & editing, Supervision.

- Darya Ahmadova: Data curation, Investigation, Validation, Writing – review & editing.

- Sandeep Sharma: Formal analysis, Investigation, Validation, Writing – review & editing.

- Sanjeev Singh: Investigation, Resources, Validation, Writing – review & editing.

- Qasem Kharmah: Formal analysis, Validation, Writing – review & editing, Supervision.

# Declaration of interests

The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

# Funding

The authors did not receive support from any organization for the submitted work.

# References

1.	Yi Wang, W., et al., Integrated computational materials engineering for advanced materials: A brief review. Computational Materials Science, 2019. 158: p. 42-48.

2.	Bordonhos, M., et al., Multiscale Computational Approaches toward the Understanding of Materials. Advanced Theory and Simulations, 2023. 6(10): p. 2200628.

3.	Xi, S., et al., Phase diagram construction and prediction method based on machine learning algorithms. Journal of Materials Research and Technology, 2025. 36: p. 1917-1929.

4.	Liu, S., et al., A comparative study of predicting high entropy alloy phase fractions with traditional machine learning and deep neural networks. npj Computational Materials, 2024. 10(1): p. 172.

5.	Connolly, J.A.D., A primer in gibbs energy minimization for geophysicists. Petrology, 2017. 25(5): p. 526-534.

6.	Kim, S.W., et al., Estimating the phase volume fraction of multi-phase steel via unsupervised deep learning. Scientific Reports, 2021. 11(1): p. 5902.

7.	Xie, C., et al., From processing text to counterfactual steel design: a knowledge-graph-organized and reliability-aware machine learning framework. Materials & Design, 2026: p. 116691.

8.	Tahkola, M., et al., Accelerated discovery of Cr-based A2+B2 superalloys across 11 elements with a deep-learning CALPHAD surrogate. npj Computational Materials, 2026.

9.	Li, S., et al., Unsupervised Machine Learning Guides the Design of MnFeCoNiMg High-Entropy Alloys for Optimizing MoS2 Interface Properties. Journal of Materials Research and Technology, 2026.

10.	Vazquez, G., et al., A deep neural network regressor for phase constitution estimation in the high entropy alloy system Al-Co-Cr-Fe-Mn-Nb-Ni. npj Computational Materials, 2023. 9(1): p. 68.

11.	Yu, W., et al., Integrated design of hardness and weldability for multi-component Fe-based hardfacing alloys driven by machine learning and high-throughput computation. Journal of Materials Research and Technology, 2026. 42: p. 11496-11509.

12.	Mayr, L.M. and D. Bojanic, Novel trends in high-throughput screening. Current Opinion in Pharmacology, 2009. 9(5): p. 580-588.

13.	Zhang, T., et al., A self-adaptive deep learning algorithm for accelerating multi-component flash calculation. Computer Methods in Applied Mechanics and Engineering, 2020. 369: p. 113207.

14.	Ben Hicham, K.K., et al., Differentiable Thermodynamic Phase-Equilibria for Machine Learning. Journal of Chemical Information and Modeling, 2026.

15.	Meloni, F., et al., Integrating Compositional Data Analysis (CoDA) and Random Forest for lithology-specific geochemical baseline determination. Science of The Total Environment, 2026. 1011: p. 181169.

16.	Parent, L.E., Compositional and Machine Learning Tools to Model Plant Nutrition: Overview and Perspectives. Horticulturae, 2025. 11(2): p. 161.

17.	Karthik, M.R. and T.B. Rao, Physics-informed data-driven ensemble and transfer learning approaches for prediction of temperature field and cutting force during machining IN625 superalloy. International Journal on Interactive Design and Manufacturing (IJIDeM), 2025. 19(10): p. 7027-7060.

18.	Agrawal, A. and A. Choudhary, Perspective: Materials informatics and big data: Realization of the “fourth paradigm” of science in materials science. APL Materials, 2016. 4(5).

19.	Ward, L. and C. Wolverton, Atomistic calculations and materials informatics: A review. Current Opinion in Solid State and Materials Science, 2017. 21(3): p. 167-176.

20.	Li, K., et al., Probing out-of-distribution generalization in machine learning for materials. Communications Materials, 2025. 6(1): p. 9.

21.	Segal, N., et al., Known Unknowns: Out-of-Distribution Property Prediction in Materials and Molecules. npj Computational Materials, 2025. 11(1): p. 345.

22.	Li, X., et al., Combining transfer learning and statistical measures to predict performance of composite materials with limited data. Computer-Aided Civil and Infrastructure Engineering, 2025. 40(6): p. 817-838.

23.	Hatakeyama-Sato, K. and K. Oyaizu, Generative Models for Extrapolation Prediction in Materials Informatics. ACS Omega, 2021. 6(22): p. 14566-14574.

24.	Speckhard, D.T., et al., Extrapolation to the complete basis-set limit in density-functional theory using statistical learning. Physical Review Materials, 2025. 9(1): p. 013801.

25.	Li, Y., et al., Towards high-throughput microstructure simulation in compositionally complex alloys via machine learning. Calphad, 2021. 72: p. 102231.

26.	Rahnama, A., S. Clark, and S. Sridhar, Machine learning for predicting occurrence of interphase precipitation in HSLA steels. Computational Materials Science, 2018. 154: p. 169-177.

27.	Hao, S., et al., Developing reliable machine learning interatomic potential for Fe–Cr–Ni austenitic alloys. Journal of Applied Physics, 2025. 138(8).

28.	Panchal, J.H., S.R. Kalidindi, and D.L. McDowell, Key computational modeling issues in Integrated Computational Materials Engineering. Computer-Aided Design, 2013. 45(1): p. 4-25.

29.	Song, Y., et al., Prediction of clathrate hydrate phase equilibria using gradient boosted regression trees and deep neural networks. The Journal of Chemical Thermodynamics, 2019. 135: p. 86-96.

30.	Eiken, J., B. Böttger, and I. Steinbach, Multiphase-field approach for multicomponent alloys with extrapolation scheme for numerical application. Physical Review E—Statistical, Nonlinear, and Soft Matter Physics, 2006. 73(6): p. 066122.

31.	Anburaj, J., et al., Ageing of forged superaustenitic stainless steel: Precipitate phases and mechanical properties. Materials Science and Engineering: A, 2012. 535: p. 99-107.

32.	Aditya, D.M., et al., The study of sigma and carbide in cast austenitic stainless-steel grade HH after 24 years of high-temperature service. Heliyon, 2023. 9(3).