## Slide 1
Validated High-Throughput Screening
with simplex-constrained surrogates for CALPHAD phase-fraction prediction in nine alloy systems
1
CALPHAD data → constrained heads
Five Fe-based ternary systems
Fe–Cr–Ni · Fe–Cr–Mn · Fe–Cr–Mo
Fe–Cr–V · Fe–Mn–Ni
pycalphad + MatCalc steel DB
44,397 validated equilibria · 3 seeds
targets: Nᵏ ≥ 0, Σ Nᵏ = 1
Fe
x₂
x₃
One fixed protocol, three seeds
constrained MLP (3 × 192): six output heads
sigmoid · residue · sparsemax · softmax ·
sigmoid/Σ · renorm
baselines: ridge · k-NN · XGBoost · random forest
Simplex closure: predicted phase fractions
one test point
BCC
FCC
LIQ
σ
on-simplex heads
Σ = 1
post-hoc renorm
Σ = 1
unconstrained sigmoid
Σ ≈ 1.07
closure ≠ simplex validity: the residue head closes the sum yet emits negative fractions on up to 1.2 % of cells
✓
structural constraints: Σ ŷ = 1 at no accuracy cost
✗
no single architecture wins all five systems
Test MAE, best MLP vs random forest
MLP
forest
Fe–Cr–Ni
MLP wins
Fe–Cr–Mn
MLP wins
Fe–Cr–Mo
tie
Fe–Cr–V
tie
Fe–Mn–Ni
RF wins
2
Spatial holdout vs. controls
Two spatial protocols + controls
contiguous interior-band holdout
T ∈ [1200, 1400] K
strict one-sided extrapolation
x₂: ≤ 0.25 → > 0.35
train
held out / far side
+ size-matched random control
Composition-band penalty, Fe–Cr–Ni
band MAE ÷ matched random-control MAE
constrained MLP
1.61×
XGBoost
2.24×
random forest
3.11×
held-out band lies 99.3–99.4 % inside the training convex hull — interior generalization, not extrapolation
Strict one-sided extrapolation
trees
MLP
MAE
training range edge
coordinate
all evaluated families degrade sharply beyond the training range; the MLP degrades least — yet none extrapolates reliably
Constrained MLPs degrade more gracefully than trees under contiguous region holdout: the region-matched penalty is smaller for MLPs in 9 of 10 band × system combinations. Graceful degradation is not reliable extrapolation.
3
Regression vs. phase detection
Two distinct tasks, one prediction
regression (MAE)
BCC
FCC
LIQ
σ
detection (F₁)
×
BCC
FCC
LIQ
σ
rare phases are cheap in aggregate MAE — zero-fraction rows contribute almost no error
Fe–Mn–Ni: the ranking reverses
test MAE (lower is better)
RF
0.0058
MLP
0.0140
forest wins
rare-phase detection (MNNI · MNNI2 · ALPHA_MN)
RF
resolves 2 of 3
MLP
×
×
×
detects none
forest wins
the best regressor need not be the best detector
Robust to the presence threshold
10⁻⁴
10⁻³
10⁻²
gap persists at all three
although the detector ranking flips with the threshold on Fe–Cr–Mo
Report both. Low phase-fraction MAE does not imply good phase-presence detection — for alloy design, detecting a rare phase matters as much as estimating its fraction.
Fixed-protocol benchmark · 6 heads + 2 mechanism probes · 4 baselines · 5 ternary + 4 extension systems · 88,542 equilibria · seeds 42 / 123 / 2024 · negative results reported in full